Effect of various types of Dyes and N-doping in supporting performance of TiO2 based Dye Sensitized Solar Cells

Shivam Yadav1, Vinita Dhulia1

1N.E.S Ratnam College of Arts Science and Commerce, Mumbai, Maharashtra, India.

Corresponding Author: shivam.yadav@ratnamcollege.edu.in

# Abstract

Dye Sensitised Solar Cell (DSSC) have piqued both practical and theoretical attention since they emerged as low-cost alternative to conventional silicon based solar cell[1][2]. TiO2 nanoparticles are abundant, stable, and nontoxic and they are widely employed for a variety of applications[3]. The band gap of TiO2 is determined to be about 3.2 eV for the anatase phase, which restricts the visible light absorption. Here we have analysed the absorption spectra for the pure TiO2 and compared it with that of N-doped TiO2 using a UV-visible spectrophotometer. Absorption spectra were also observed for composites of TiO2 made by varying the concentration of Nitrogen[7]. Synthesis of TiO2 and N-doped TiO2 was done using Sol-gel method [4][5][6]. Particle size for TiO2 was confirmed using X-Ray Diffraction.

It was observed that Nitrogen doping reduces the band gap leading to increase in the absorption of light in visible range. Further studies were carried out by adding four different Azo dyes as a sensitizer for N-doped TiO2. I-V Characterisation of the samples was examined to determine their effectiveness. The best result was found with Methylene Blue.

Keywords: Dye Sensitised Solar Cell (DSSC), Azo Dye, TiO2 Nano-particles, N-doped TiO2, Energy band gap.

- Introduction

O’Regan and Grätzel reported that the Dye-Synthesized Solar Cell (DSSC) is a promising alternative to silicon and multi-junction solar cells[8]. DSSC is a device that converts photons into electrons[1][9]. The Dye used as a photosensitizer has a significant impact on the DSSC's performance[10]. This is because it absorbs more light than TiO2 alone and converts photons to electrons, resulting in a higher photon to electron conversion efficiency[7].

The advantages of Azo dyes include their availability and low cost. For a dye to efficiently convert light to electricity in DSSC, the Lowest Unoccupied Molecular Orbital (LUMO) must have a more negative potential than TiO2’s conduction band edge, allowing the injection process to be thermodynamically favourable. Furthermore, the dye must be in a good electrical and chemical contact with TiO2 for electron injection to be efficient. The Highest Occupied Molecular Orbital (HOMO) of the dye must be more positive. Finally, the band gap of the dye must be as small as possible[2][11][12].

- Experimental Work

2.1	 Synthesis of TiO2 and Nitrogen doped TiO2 Nanoparticles by Sol-Gel method

By using the Sol-Gel method, we have prepared samples of TiO2 nanoparticles, pure TiO2 and Nitrogen doped TiO2[4][6][13]. Four different Azo dyes were obtained from Loba Chemicals: Methyl Orange, Methylene Blue, Eriochrome Black T and Alizarin Red. Titanium butoxide (C16H36O4Ti) precursor used for TiO2 nanoparticles synthesis, Ethanol (C2H5OH), De-ionized water, and Nitric acid (HNO3) are taken in the ratio 1/20/0.5/0.1 respectively [13]. It was maintained at 450oC for annealing. N-doped TiO2 is obtained using TiO2 nanoparticles and Tri-ethylamine (Nitrogen source) taken in equal ratios. Composites were also prepared with TiO2 and 4 different Azo dyes taken in a ratio of 1:1 and also N-doped TiO2 with Azo dyes taken in a ratio of 1:1.

2.2	Characterization of the Composites

2.2.1 Size of the TiO2 Nanoparticles using XRD

X-Ray Powder Diffraction (XRD) patterns for the pure TiO2 sample were collected and the crystal size of samples was calculated from peak broadening by the Scherrer equation.

2.2.2 Absorption Spectra of the composites

The absorption Spectra was studied using UV visible spectrophotometer first with pure TiO2 and N-doped TiO2, composites of TiO2 with all four dyes taken in the ratio of 1:1, composites of N-Doped TiO2 with all four dyes taken in ratio 1:1.

3	Results and Discussion

3.1	X-Ray Diffraction (XRD)

Figure1: XRD of Pure TiO2

Figure 1 shows the X-Ray Diffraction pattern of Pure TiO2. Diffraction peaks of Pure TiO2 were obtained at 25.320, 37.870, 48.0560, 53.910, 55.080, 62.70, 68.760, 70.310, and 75.120. These can be assigned to crystal planes (101), (004), (200), (105), (211), (204), (116), (220) and (215) that correspond to the anatase phase of titania and agree with JCPDS card np.21-1272.

The average crystalline particle size is calculated by applying Sherer expressions in equation (1)

D=0.9 λβ.COSϴ----(1)

Table 1 The average particle size of the sample

| Sample | 2θ | FWHM (Full Width Half Maxima) | Average particle size(nm) |
| --- | --- | --- | --- |
| Pure TiO2 | 25.302 | 0.6177 | 13 |

The λ is X-Ray wavelength of 1.5406 Å of Cu kα radiation. β is the line broadening at maximum intensity (FWHM) and θ is the Bragg angle. The particle size is recorded in the table.

3.2 	UV-Visible Spectroscopy

The Optical measurement was made using UV-VIS Spectrophotometer for the dyes and the composites of dyes with Pure TiO2 and N-doped TiO2 for the mixing ratio (1:1). The absorption Spectra showed the presence of distinct absorption peaks in the visible region for each type of dye.

Image1: Azo Dyes At 1000 PPM               Image2: Dyes with Pure TiO2           	      Image3: Dyes with N-Doped TiO2

Figure2: Absorption Specta of all the 4 dyes 		                                Figure3: Absorption Spectra of Pure TiO2 with all 4

dyes (1:1 Ratio)

Figure4: Absorption Spectra of N-doped TiO2 with           Figure5: Absorption Spectra of Pure TiO2

all 4 dyes (1:1 Ratio)				 and N-doped TiO2

It is evident from the characterization that as nitrogen is introduced, the absorbance edge shifts, resulting in a smaller band gap. As a result, the N-doped TiO2 sample had a greater absorption of visible light. Similarly, narrowing the band gap of TiO2 leads to less charge recombination as compared to pure TiO2.

Using the Kubelka-Munk formula[14] from equation (2), UV-Visible Spectra are transformed into Tauc plots to determine the band gap of the doped sample.

αhv=A(hv-Eg)2----(2)

where α is absorbance coefficient, h is the Plank’s constant (4.136*10-15eV), A is constant (̴1), v is frequency and Eg is band gap.

3.3	Band Gap

Figure 6: Band-Gap of Pure and N-doped TiO2

Figure7: Bandgap of Pure TiO2 with all 4 Dyes                    Figure8: Bandgap of 8% N-doped TiO2 with all 4 Dyes

Table 2 Bandgap energy for all samples

| Sample | Band Gap (eV) |
| --- | --- |
| Pure TiO2 | 3.05 |
| 6% doped TiO2 | 2.92 |
| 8% doped TiO2 | 2.73 |
| 8% doped TiO2 with Methylene Blue | 1.63 |

Figure 6 shows the narrowing of the band-gap for N-doped TiO2. Figure 7 and 8 show that TiO2 with all the four dyes has enhanced absorption in visible region and narrowed band-gap maximum absorption was observed for Methylene Blue.

4	Conclusion

By examining the optical characteristics, it is observed that composites of dye with pure TiO2 and N-doped TiO2 enhance the performance of DSSC. Doping of TiO2 with Nitrogen lowered its band gap. The composite of N-doped TiO2 with Methylene Blue was found to have maximum absorption.

Acknowledgement

We are thankful to N.E.S. Ratnam College for providing laboratory facilities, we would also like to thank department of Chemistry for providing the essential chemicals, Sophisticated Analytical Instrument Facility (SAIF) IIT Bombay for providing UV-Vis Spectrometer data and Doctor Nainesh Patel for providing XRD data.

References

- Ahmad, Muhammad Shakeel, Adarsh Kumar Pandey, and Nasrudin Abd Rahim. "Advancements in the development of TiO2 photoanodes and its fabrication methods for Dye Sensitized Solar Cell (DSSC) applications. A review." Renewable and Sustainable Energy Reviews 77 :89-108. (2017)

- Reghunath, Shalini, Dephan Pinheiro, and Sunaja Devi KR. "A review of hierarchical nanostructures of TiO2: Advances and applications." Applied Surface Science Advances 3 :100063. (2021)

- Dahl, Michael, Yiding Liu, and Yadong Yin. "Composite Titanium dioxide nanomaterials." Chemical reviews 114.19 :9853-9889. (2014)

- Bessekhouad, Y., D. Robert, and J. V. Weber. "Preparation of TiO2 nanoparticles by Sol-Gel route." International journal of photoenergy 5.3: 153-158. (2003)

- Sharma, Ajay, R. K. Karn, and S. K. Pandiyan. "Synthesis of TiO2 nanoparticles by sol gel method and their characterization." J Basic Appl Eng Res 1.9: 1-5. (2014)

- Sathish, M., et al. "Synthesis, characterization, electronic structure, and photocatalytic activity of Nitrogen-doped TiO2 nanocatalyst." Chemistry of materials 17.25: 6349-6353. (2005)

- Cong, Ye, et al. "Synthesis and characterization of Nitrogen-doped TiO2 nanophotocatalyst with high visible light activity." The Journal of Physical Chemistry C 111.19: 6976-6982. (2007)

- O'regan, Brian, and Michael Grätzel. "A low-cost, high-efficiency solar cell based on dye-sensitized colloidal TiO2 films." nature 353.6346 (1991): 737-740.

- Suhaimi, Suriati, et al. "Materials for enhanced dye-sensitized solar cell performance: Electrochemical application." Int. J. Electrochem. Sci 10.4 (2015): 2859-2871.

- Ludin, Norasikin A., et al. "Review on the development of natural dye photosensitizer for dye-sensitized solar cells." Renewable and Sustainable Energy Reviews 31 (2014): 386-396.

- Shalini, Status, et al. "Status and outlook of sensitizers/dyes used in dye sensitized solar cells (DSSC): a review." International journal of energy research 40.10 (2016): 1303-1320.

- Shalini, Status, et al. "Status and outlook of sensitizers/dyes used in dye sensitized solar cells (DSSC): a review." International journal of energy research 40.10 (2016): 1303-1320.

- Fernandes, R., et al. "Low energy ion-beam modification of TiO2 photocatalyst thin film for visible light absorption." Surface and Coatings Technology 203.17-18 (2009): 2579-2583.

- Yang, Li, and Björn Kruse. "Revised Kubelka–Munk theory. I. Theory and application." JOSA A 21.10 (2004): 1933-1941.