Spectroscopic Properties of Dy3+ Doped Lead Lithium Cadmium Tantalum

Magnesium Bismuth Borate Glasses

S.L.Meena

Ceramic Laboratory, Department of physics, Jai Narain Vyas University, Jodhpur 342001(Raj.) India

E-mail address:shankardiya7@rediffmail.com

Abstract

Glass sample of Lead Lithium Cadmium Tantalum Magnesium Bismuth Borate (35-x) Bi2O3:10PbO:10Li2O:10CdO:10Ta2O5:10MgO:15B2O3: x Dy2O3.  (where x=1,1.5 and 2 mol%) have been prepared by  melt-quenching technique.  The amorphous nature of the prepared glass samples was confirmed by X-ray diffraction. Optical absorption and fluorescence spectra were recorded at room temperature for all glass samples. Judd-Ofelt intensity parameters Ωλ (λ=2, 4 and 6) are evaluated from the intensities of various absorption bands of optical absorption spectra. Using these intensity parameters various radiative properties like spontaneous emission probability, branching ratio, radiative life time and stimulated emission cross–section of various emission lines have been evaluated

Keywords: LLCTMBB Glasses, Optical Properties, Judd-Ofelt Theory, Rare earth ions.

I. Introduction

Bismuth borate glasses doped with trivalent rare-earth ions are very important because they show strong luminescence due to their small cutoff phonon frequencies and scientific application [1-4].Rare earth doped bismuth borate glasses and glass ceramics are of increasing interests in various optical applications, because of their optical, liner and non liner properties. The performance and relatively low cost of borate glasses make them attractive for most of the ordinary laser applications [5-7].

Among various glasses, borate glasses are excellent host matrices because boric oxide (B2O3) acts as a good glass former and flux material. The structure of vitreous B2O3 consists of a random network of boroxyl rings and BO3 triangles connected by B-O-B linkages. Borate glass forming ability over wide range of composition, higher bond strength, high transparency, low melting point and good rare earth ion solubility [8, 9]. The addition of network modifier (NWF) Li2O is to improve both electrical and mechanical properties of such glasses. With the presence of property modifying (MgO) with B2O3 glass network could significantly improve different properties like mechanical strength, thermal stability and chemical durability [10-14].

The present work reports on the preparation and characterization of rare earth doped heavy metal oxide (HMO) glass systems for lasing materials. We have studied on the absorption and emission properties of Dy3+ doped lead lithium cadmium tantalum magnesium bismuth borate glasses. The intensities of the transitions for the rare earth ions have been estimated successfully using the Judd-Ofelt theory, The laser parameters such as radiative probabilities(A),branching ratio (β), radiative life time(τR) and stimulated emission cross section(σp) are evaluated using J.O.intensity parameters( Ωλ, λ=2,4 and 6).

II. Experimental Techniques

Preparation of glasses

The following Dy3+doped bismuth borate glass samples (35-x) Bi2O3:10 PbO: 10Li2O:10 CdO: 10Ta2O5: 10MgO: 15B2O3: xDy2O3.  (where x=1,1.5 and 2 mol%)  have been prepared by melt-quenching method. Analytical reagent grade chemical used in the present study consist of Bi2O3, PbO, Li2O, CdO, Ta2O5, MgO, B2O3 and Dy2O3. They were thoroughly mixed by using an agate pestle mortar. then melted at 10500C by an electrical muffle furnace for 2h., After complete melting, the melts were quickly poured in to a preheated stainless steel mould and annealed at temperature of 3500C for 2h to remove thermal strains and stresses. Every time fine powder of cerium oxide was used for polishing the samples. The glass samples so prepared were of good optical quality and were transparent. The chemical compositions of the glasses with the name of samples are summarized in Table 1.

Table 1.

Chemical composition of the glasses

Sample     	Glass composition (mol %)

LLCTMBB (UD)      35Bi2O3:10PbO:10Li2O:10CdO:10Ta2O5:10MgO:15B2O3.

LLCTMBB (DY1)    34Bi2O3:10PbO:10Li2O:10CdO:10Ta2O5:10MgO:15B2O3.1 Dy2O3.

LLCTMBB (DY1.5) 33.5Bi2O3:10PbO:10Li2O:10CdO:10Ta2O5:10MgO:15B2O3.1.5 Dy2O3.

LLCTMBB (DY2)    33Bi2O3:10PbO:10Li2O:10CdO:10Ta2O5:10MgO:15B2O3.  2 Dy2O3.

LLCTMBB (UD) -Represents undoped   Lead Lithium Cadmium Tantalum Magnesium Bismuth Borate glass specimens.

LLCTMBB (DY)-Represents Dy3+ doped   Lead Lithium Cadmium Tantalum Magnesium Bismuth Borate glass specimens.

III.Theory

3.1 Oscillator Strength

The intensity of spectral lines are expressed in terms of oscillator strengths using the relation [15].

fexpt. = 4.318 ×10-9∫ε (ν) d ν                                          (1)

where, ε (ν) is molar absorption coefficient at a given energy ν (cm-1), to be evaluated from Beer–Lambert law.

Under Gaussian Approximation, using Beer–Lambert law, the observed oscillator strengths of the absorption bands have been experimentally calculated [16], using the modified relation:

Pm=4.6 ×10-9×log ×Δυ1/2                                                          (2)

where c is the molar concentration of the absorbing ion per unit volume, I is the optical path length, logI0/I is optical density and Δυ1/2 is half band width.

3.2. Judd-Ofelt Intensity Parameters

According to Judd [17] and Ofelt [18] theory, independently derived expression for the oscillator strength of the induced forced electric dipole transitions between an initial J manifold │4fN (S, L) J> level and the terminal J’ manifold │4fN (S', L') J'> is given by:

(3)                                                        Where, the line strength S (J, J') is given by the equation

S (J, J') =e2 ∑ Ωλ<4f N(S, L) J║U (λ) ║4fN (S', L') J'>2                   (4)

λ =2, 4, 6

In the above equation m is the mass of an electron, c is the velocity of light, ν is the wave number of the transition, h is Planck’s constant, n is the refractive index, J and J' are the total angular momentum of the initial and final level respectively, Ωλ (λ=2,4and 6) are known as Judd-Ofelt intensity parameters.

3.3 Radiative Properties

The Ωλ parameters obtained using the absorption spectral results have been used to predict radiative properties such as spontaneous emission probability (A) and radiative life time (τR), and laser parameters like fluorescence branching ratio (βR) and stimulated emission cross section (σp).

The spontaneous emission probability from initial manifold │4fN (S', L') J'> to a final manifold │4fN (S, L) J >| is given by:

A [(S', L') J'; (S, L) J] = 64 π2ν33h2J'+1nn2+229×S(J',J)                       (5)

Where, S (J', J) = e2 [Ω2║U (2) ║2 + Ω4║U (4) ║2 + Ω6║U (6) ║2]

The fluorescence branching ratio for the transitions originating from a specific initial manifold │4fN (S', L') J'> to a final many fold│4fN (S, L) J > is given by

β [(S', L') J'; ( S , L ) J ] =  AS'  L AS' L' J'S  L(6)

S L J

where, the sum is over all terminal manifolds.

The radiative life time is given by

 rad  A[(S', L') J'; (S,L ) ]  = ATotal-1                                       (7)

S L J

where, the sum is over all possible terminal manifolds. The stimulated emission cross -section for a transition from an initial manifold │4f N (S', L') J'> to a final manifold

│4fN (S, L) J >| is expressed as

σpλp=λp48πcn2Δλeff ×AS',L' J';S, LJ                         (8)

where, λp the peak fluorescence wavelength of the emission band and Δλeff is the effective fluorescence line width.

IV. Result and Discussion

4.1 XRD Measurement

Figure 1 presents the XRD pattern of the sample contain - Bi2O3 which is show no

sharp Bragg’s peak, but only a broad diffuse hump around low angle region. This is the clear indication of amorphous nature within the resolution limit of XRD instrument

Fig. (1) X-ray diffraction pattern of   Bi2O3: PbO: Li2O: CdO: Ta2O5: MgO: B2O3: Dy2O3.

4.2 Absorption Spectrum

The absorption spectra of Dy3+doped LLCTMBB glass specimens have been presented in Figure 2 in terms of Intensity versus wavelength. Thirteen  absorption bands have been observed from the ground state 6H15/2 to excited states 6H13/2, 6H11/2, 6H9/2+6F11/2,6H7/2+6F9/2,6F7/2+6H5/2,6F5/2,6F3/2,6F9/2,4I15/2,4G11/2, 6F7/2+4I13/2, 6M19/2+4(P,D)3/2 and 4G9/2+6P3/2 for Dy3+doped LLCTMBB glasses.

Fig. (2) Absorption spectrum of Dy3+doped LLCTMBB glasses

The experimental and calculated oscillator strength for Dy3+ ions in LLCTMBB glasses are given in Table 2.

Table 2: Measured and calculated oscillator strength (Pm×10+6) of Dy3+ions in LLCTMBB glasses.

| Energy level from 6H15/2 | Glass LLCTMBB (DY01) |  | Glass LLCTMBB (DY1.5) |  | Glass LLCTMBB (DY02) |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Pexp. | Pcal. | Pexp. | Pcal. | Pexp. | Pcal. |
| 6H13/2 | 1.95 | 2.34 | 1.93 | 2.33 | 1.90 | 2.32 |
| 6H11/2 | 1.32 | 1.91 | 1.30 | 1.90 | 1.26 | 1.87 |
| 6H9/2+6F11/2 | 10.15 | 10.04 | 10.12 | 10.01 | 10.07 | 9.96 |
| 6H7/2+6F9/2 | 5.45 | 5.14 | 5.42 | 5.12 | 5.40 | 5.10 |
| 6F7/2+6H5/2 | 4.62 | 4.58 | 4.60 | 3.56 | 4.56 | 3.52 |
| 6F5/2 | 1.20 | 1.59 | 1.18 | 1.57 | 1.16 | 1.55 |
| 6F3/2 | 0.19 | 0.30 | 0.17 | 0.29 | 0.13 | 0.28 |
| 6F9/2 | 0.26 | 0.27 | 0.24 | 0.26 | 0.22 | 0.25 |
| 4I15/2 | 0.24 | 0.66 | 0.21 | 0.65 | 0.18 | 0.64 |
| 4G11/2 | 0.18 | 0.17 | 0.16 | 0.16 | 0.13 | 0.15 |
| 6F7/2+4I13/2 | 3.35 | 3.56 | 3.32 | 3.54 | 3.28 | 3.51 |
| 6M19/2+4(P,D)3/2 | 7.85 | 9.99 | 7.82 | 9.98 | 7.78 | 9.97 |
| 4G9/2+6P3/2 | 1.50 | 1.99 | 1.46 | 1.98 | 1.42 | 1.95 |
| r.m.s. deviation | 0.7287 |  | 0.7361 |  | 0.7531 |  |

*Low r.m.s. deviation values clearly indicate the accuracy of fitting.

In the Lead Lithium Cadmium Tantalum Magnesium Bismuth Borate glasses Ω2, Ω4 and Ω6 parameters decrease with the increase of x from 1 to 2 mol%. The order of magnitude of Judd-Ofelt intensity parameters is Ω2>Ω4> Ω6 for all the glass specimens. The high values obtained for Ω2 in all glasses indicate that the Dy3+ ion is subjected to higher covalency with low symmetry. The spectroscopic quality factor (Ω4 /Ω6) related with the rigidity of the glass system has been found to lie between 1.298 and 1.346 in the present glasses.

The values of Judd-Ofelt intensity parameters are given in Table 3.

Table 3: Judd-Ofelt intensity parameters for Dy3+ doped LLCTMBB glass specimens

| Glass Specimen | Ω2(pm2) | Ω4(pm2) | Ω6(pm2) | Ω4 /Ω6 | Ref. |
| --- | --- | --- | --- | --- | --- |
| LLCTMBB (DY01) | 2.362 | 1.467 | 1.130 | 1.298 | P.W. |
| LLCTMBB (DY1.5) | 2.352 | 1.468 | 1.118 | 1.313 | P.W. |
| LLCTMBB (DY02) | 2.326 | 1.479 | 1.099 | 1.346 | P.W. |
| NLTB(DY) | 9.86 | 3.39 | 2.41 | 1.407 | [19] |
| LLTB(DY) | 8.75 | 2.62 | 2.07 | 1.266 | [20] |
| PKMAF(DY) | 7.04 | 1.73 | 1.57 | 1.102 | [21] |

4.3 Excitation Spectrum

The Excitation spectra of Dy3+doped LLCTMBB glass specimens have been presented in Figure 3 in terms of Excitation Intensity versus wavelength. The excitation spectrum was recorded in the spectral region 315–465 nm fluorescence at 575nm having different excitation band centered at 322,353, 365, 385, 425, 454 and 473 nm are attributed to the 6P3/2, 6P7/2, 4P3/2, 4I13/2, 4G11/2, 4I15/2 and 4F9/2 transitions, respectively. The highest absorption level is 4I13/2 and is at 385nm.So this is to be chosen for excitation wavelength.

Fig. (3) Excitation spectrum of doped with Dy3+ LLCTMBB glasses.

4.4. Fluorescence Spectrum

The fluorescence spectrum of Dy3+doped in Lead Lithium Cadmium Tantalum Magnesium Bismuth Borate glass is shown in Figure 4. There are three broad bands observed in the Fluorescence spectrum of Dy3+doped Lead Lithium Cadmium Tantalum Magnesium Bismuth Borate glass. The wavelengths of these bands along with their assignments are given in Table 6. The peak with maximum emission intensity appears at 485nm, 575 nm and 665 nm and corresponds to the (4F9/2→6H15/2), (4F9/2→6H13/2) and (4F9/2→6H11/2) transition.

Fig. (4). Fluorescence spectrum of doped with Dy3+ LLCTMBB glasses.

Table4: Emission peak wave lengths (λp),radiative transition probability (Arad),branching ratio (β),stimulated emission cross-section( σp) and radiative life time( τR ) for various transitions in Dy3+ doped LLCTMBB glasses.

| Transition |  | LLCTMBB DY 01 |  |  |  | LLCTMBB DY 1.5 |  |  |  | LLCTMBB DY 02 |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | λmax (nm) | Arad(s-1) | β | σp (10-20 cm2) | τR(μs) | Arad(s-1) | β | σp (10-20 cm2) | τR (μs) | Arad(s-1) | β | σp (10-20 cm2) | τR (10-20 cm2) |
| 4F9/2→6H15/2 | 485 | 97.3987 | 0.2065 | 0.165 | 2119.68 | 96.664 | 0.2058 | 0.160 | 2129.32 | 95.6674 | 0.2056 | 0.154 | 2149.53 |
| 4F9/2→6H13/2 | 575 | 338.453 | 0.7174 | 1.211 |  | 337.170 | 0.7179 | 1.175 |  | 334.045 | 0.7180 | 1.136 |  |
| 4F9/2→6H11/2 | 665 | 35.9168 | 0.07613 | 0.145 |  | 35.8005 | 0.07623 | 0.143 |  | 35.5065 | 0.07632 | 0.138 |  |
| V. Conclusion In the present study, the glass samples of composition (35-x) Bi2O3:10PbO:10 Li2O:10 CdO: 10Ta2O5:10MgO:15 B2O3:xDy2O3 (where x =1, 1.5and 2mol %) have been prepared by melt-quenching method. The value of stimulated emission cross-section (σp) is found to be maximum for the transition (4F9/2→6H13/2) for all glass specimens. This shows that (4F9/2→6H13/2) transition is most probable transition. References [1] Tanabe, S., Kang, J., Hanada, T., Soga, N.(1998).“Yellow/blue luminescence of Dy3+ doped borate glasses and their anomalous temperature variations”, J Non-Cryst Solids, 239:170. [2] Alajerami,Y.S.M., Hashim,S., Hassan,W. M. S., Ramli, A. T., Kasim, A. (2012) .Optical properties of lithium magnesium borate glasses doped with Dy3+ and Sm3+ ions, Physica B 407, 2398– 2403. [3] Kumar,M. V., Jamalaiah, B. C., Gopal, K. R., Reddy, R. R. (2012).Optical absorption and fluorescence studies of Dy3+- doped lead telluroborate glasses, J. Lumin. 132, 86-90. [4] Rajesh,D., Balakrishna,A. Ratnakaram, Y.C. (2012). Luminescence, structural and dielectric properties of Sm3+ impurities in strontium lithium bismuth borate glasses. Opt. Mat. 35, 108–116. [5] Ratnakaram, Y.C., Thirpathi, N.D. and Chakaradhar, R.P.S.(2006).Spectral studies of Sm3+ and Dy3+ doped lithium cesium mixed alkali borate glasses.J.Non-cryst.Solids,352,3914. [6]. Lin, H., Pun, E.Y.B. and Wang, X.J. (2005). Intense visible fluorescence and energy transfer in Dy3+, Tb3+, Sm3+ and Eu3+ doped rare-earth borate glasses. J. Alloy. Compd., 390,197. [7]. Rao, K.V., Babu, S. , Venkataiah, G. , Ratnakaram, Y. C. (2015) “Optical Spectroscopy of Dy3+ doped borate glasses for luminescence applications”, Journal of Molecular Structure 1094,274-280. [8] Gedam,R. S., Ramteke, D. D. (2012).Electrical and optical properties of lithium borate glasses doped with Nd2O3, J. Rare Earths 30 (8) , 785-789. [9] Gedam, R. S., Ramteke, D. D. (2013). Influence of CeO2 addition on the electrical and optical properties of lithium borate glasses, J. Phys. Chem.Solids 74, 1399-1402. [10] George, J. L. (2015). Dissolution of borate glasses and precipitation of phosphate compounds. Spring, 1-191. [11] Zang, X. M., Li, D. S., Pun,E. Y. B.,and Lin,H.(2017). Dy3+ doped borate glasses for laser illumination, Optical Material Express, Vol.7(6),pp-2040-2054. [12]. Dahiya, M.S., Khasa,S. and Agarwal,A. (2015).Physical, thermal, structural and optical absorption studies of vanadyl doped magnesium oxy-chloride bismo-borate glasses . Journal of Asian Ceramic Societies 3, 206–211. [13]. Mariselvam,K.,Kumar,A.,Anuradha,M.and Panigrahi,B.S.(2017). Synthesis and photoluminescence behaviour of dysprosiumdoped barium bismuth borate glasses.Opto. Electronocs and Adv.Material, Vol.11, pp-462-466. [14]Parandamaiah,M.(2015). Dy3+ doped Lithium Sodium Bismuth Borate Glasses for Yellow Luminescent Photonic Applications, Vol.5(8),pp.126-131. [15]. Gorller-Walrand, C. and Binnemans, K. (1988) Spectral Intensities of f-f Transition. In: Gshneidner Jr., K.A. and Eyring,L., Eds., Handbook on the Physics and Chemistry of Rare Earths, Vol. 25, Chap. 167, North-Holland, Amsterdam, 101-264. [16]. Sharma, Y.K., Surana, S.S.L. and Singh, R.K. (2009) Spectroscopic Investigations and Luminescence Spectra of Sm3+ Doped Soda Lime Silicate Glasses. Journal of Rare Earths, 27, 773. [17]. Judd, B.R. (1962). Optical Absorption Intensities of Rare Earth Ions. Physical Review, 127, 750. [18]. Ofelt, G.S. (1962). Intensities of Crystal Spectra of Rare Earth Ions. The Journal of Chemical Physics, 37, 511. [19] Saleema,S.A. , Jamalaiah, B.C., Jayasimhadri, M., Rao,A. S., Jang, K., Moorthy,L. R. (2011). Journal of Quantitative Spectroscopy & Radiative Transfer, pp.78–84. [20]S.A. Saleema, B.C. Jamalaiah, M. Jayasimhadri, A. Srinivasa Rao, Kiwan Jang, L. Rama Moorthy. “Luminescent studies of Dy3+ ion in alkali lead tellurofluoroborate glasses”, Journal of Quantitative Spectroscopy & Radiative Transfer, pp. 78–84 2011. [21]Sardar, D.K., Bradley, W.M., Yow, R.M. Gruber, J.B., Zandi, B. (2004). “Optical transitions and absorption intensities of Dy3+ (4f9) in YSGG laser host”, J Lumin, 106, pp.195–203. |  |  |  |  |  |  |  |  |  |  |  |  |  |