Removal of Rhodamine 6G from Aqueous Solution by Adsorption on Bio Adsorbent Prepared from Hyptis Suaveolens (Vilayti Tulsi): Kinetic, Equilibrium and Thermodynamic Study

N. N. GUND 1. B. M. MARMAT 1. A. S. SALUNKE 1.  J. P. SONAR 1. S. A. DOKHE 1. A. M. ZINE 1. S. N. THORE 2. S. D. PARDESHI 1*

1 Department of Chemistry, VinayakraoPatilMahavidyalaya, Vaijapur, Maharashtra 423 701, India.

2 Department of Chemistry, Deogiri College, Station Road, Aurangabad, Maharashtra 431 005, India.

*Email: sandeeppardeshi007@gmail.com * Orcid ID orcid.org/0000-0001-8794-5629

__________________________________________________________________________________

Abstract

The adsorption capacity of bio adsorbent, prepared from Hyptissuaveolens (VilaytiTulsi), for Rhodamine 6G removal from aqueous solution was investigated in the present study. The effect of ph, initial dye concentration, time, adsorbent dosage and temperature was investigated. The present adsorption follows pseudo second order kinetics. Langmuir isotherm and Freundlich isotherm was used for present study. The maximum adsorption capacity under optimum condition was found to be 48.78 mg g-1. The thermodynamics study shows endothermic, spontaneous adsorption process.

Keywords: Rhodamine 6G, Adsorption, Dye removal, Bio adsorbent.

___________________________________________________________________________

1. Introduction

Different chemical material were used in various industrial processes. Dyes are the mostly used organic chemical in the industries such as paper and pulp, lather, textile etc. Residual part of dyes comes in effluent of such industries creating environment problem [1, 2]. Most of the organic dyes are highly toxic and carcinogenic [3-5]. The presence of dyes can seriously affect the light penetration and damage the aquatic life [6]. There are different methods available for removal of hazardous dyes such as photo degradation and photo catalysis [7-10], electrochemical degradation [11], bio degradation [12, 13], chemical coagulation and adsorption. Among all adsorption have been the most common method employed for dye removal [14-16]. Activated carbon is the most suitable adsorbent but it is quite expensive so alternate cheaper adsorbent is a need [17-18].

Literature survey shows that different adsorbent have been reported for dye removal some of them are nanomaterials [19] such as magnetite@graphene oxide [20] Carbon nanotubes [21], CoFe2O4/rGO nanocomposite [22] while some are prepared from natural material such as Moroccan natural phosphate [23], activated carbon prepared from Prosopisspicigera L. wood [24], rice husk [25, 26], Clitoriafairchildiana pods [27], Prunusamygdalus L. [28] etc.

Rhodamine 6G is a fluorescent basic dye mainly used to coloured wool, cotton, silk etc. It is toxic and carcinogenic in nature [8, 29], so this dye was selected for present study.

2. Experimental

2.1Preparation of Adsorbent

Fully grown plants of Hyptissuaveolens (VilaytiTulsi) were collected around Vaijapur city. The steams and braches were cut into small pieces, washed with distilled water for 2-3 times, dried under shed. The adsorbent was prepared as per the procedure mentioned in our earlier publication [30].

2.2 Preparation of sorbet

Rhodamine 6G (Rh 6G), a cationic dye supplied by LobaChem India with Colour Index (C.I.) 45,160 and molecular formula C28H31N2O3Cl was used for present study. A stock solution of 1000 mg L-1 was prepared by dissolving accurately weigh dye quantity in double distilled water. Dilution with double distilled was carried out to get desired experimental concentration.

2.3 Adsorption Studies

For adsorption studies, in 250 mL stoppered glass bottle 50 mL dye solution of desired concentration and pH was taken at room temperature. 0.1 g adsorbent was added, the solution was stirred by mechanical shaker. At predetermined time interval, the small fraction were withdrawn, the dye solution was separated from adsorbent by centrifugation at 4,000 rpm. The absorption of supernatant solution was measured. The standard curve of dye was prepared with 1-9 mgL-1 solution at 526 nm using Elico double beam spectrophotometer SL-210. 0.1 M HCl and 0.1 M NaOH was used to control initial pH. Different adsorbent dosage (0.05 to 0.3 g) and 50 mL of 50 mgL-1 dye solution was shaken for 30 min to study effect of adsorbent dosage. Effect of temperature was studied by adding 0.1 g adsorbent in 50 mL dye solution of 25 mgL-1, 50 mgL-1, 75 mgL-1 and 100 mgL-1 concentration at 313, 323 and 333 0K in thermostat rotatory shaker. The following equation was used to determine the solid phase dye concentration at time.

qt=C0-CtVW						(1)

whereqt is adsorption amount at time t, Co and Ct are dye concentration initial and at time t in mg L-1 respectively, V is volume of solution in L and W is weight of adsorbent in g. The adsorption capacity of adsorbent was determined by using Langmuir and Freundlich isotherm.

3 Results and Discussion

3.1 Effect of pH

Initial pH of the dye solution is the most dominant parameter that affect the adsorption capacity of the adsorbent [31]. The initial pH of solution affect the adsorption procedure as it affect the ionization of dyes and adsorbent surface [14]. To study the effect of pH, 50 mL solution of 50mg L-1 dye concentration was shaken with 0.1g adsorbent for 30 min. An increase in pH from 4 to 7.5 increases the adsorption of Rhodamine 6G (16.14 to 20.19 mg g-1) further increase in pH from 7.5 to 10 slightly decreases the adsorption. The optimum pH is 7.5. Fig.1 shows the effect of pH on adsorption.

Fig 1. Effect of pH on dye removal

3.2 Effect of Adsorbent dose

To test the effect of adsorbent dose, 50 mg L-1 dye concentration was stirred with varying adsorbent amount (0.05 to 0.3 g) at optimum pH for 30 min. the result was shown in Fig.2. It has been observed that due to increase in adsorption site the % removal of dye increases but unit adsorption was decreased from 39.7 mg g-1 to 7.18 mg g-1 as amount of adsorbent was increased from 0.05 g to 0.3 g.

Fig. 2 Effect of Adsorbent dose

3.3 Effect of dye concentration

To study the effect of initial dye concentration, 50mL dye solution with varying concentration (25 mg L-1 to 100 mg L-1) was stirred with 0.1 g adsorbent at optimum pH (7.5). The results are shown in Fig.3, as the initial dye concentration increases the percentage removal of dye decreases, but the unit adsorption increases from 10.27 mg g-1 to 48.72 mg g-1.

Fig. 3 Effect of initial dye concentration on adsorption

3.4 Adsorption dynamics

3.4.1 The pseudo first order kinetic model

The pseudo first order kinetic model expression is given by Lagergren [32] as follows

logqe-qt=logqe-k1t2.303					(2)

Where qt and qe are amount of dye adsorbed at time t and equilibrium, respectively k1 is the rate constant. Fig. 4 shows the Lagergren pseudo first order plot for adsorption of Rh 6G at various initial concentration. The values of k1 and qe were calculated from slope and intercept from plot of log (qe-qt) versus t and represented in table1. The experimental data with Lagergren pseudo first order plot provide poor correlation coefficient (R2) values similar inapplicability was also observe by Lata et al [33].

Fig. 4 The pseudo first order kinetic

3.4.2 The pseudo second order kinetic model

The pseudo second order Lagergren equation is expressed as [34]

tqt=1qe2k2+tqt						(3)

Plot of t/qtversus t was shown in the Fig.5. From the slopes and intercepts, values of equilibrium adsorption capacity (qe) and second order rate constant (k2) were determined and expressed in table 1. From the values of regression coefficient it can be concluded that the present system follows pseudo second order Lagergren model. The adsorbent and adsorbate both affect the adsorption process of present study [35].

Fig. 5 The pseudo second order kinetic

Table 1 Rate constants for pseudo first-order and pseudo second-order adsorption

| Conc. C0 (mg L-1) | pseudo first-order |  |  | pseudo second-order |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | qe (mg g-1) | K1 (min-1) | R2 | qe (mg g-1) | K2 (min-1) | R2 |
| 25 | 2.186 | 0.0476 | 0.9244 | 10.537 | 0.0472 | 0.999 |
| 50 | 1.7290 | 0.0536 | 0.9680 | 24.390 | 0.2302 | 1 |
| 75 | 5.2432 | 0.0391 | 0.9612 | 36.363 | 0.5817 | 1 |
| 100 | 13.749 | 0.0244 | 0.9124 | 48.780 | 1.4008 | 1 |

3.5 Adsorption equilibrium study

Two isotherm, Langmuir isotherm and Freundlich isotherm was used for present study.

3.5.1 Langmuir isotherm

Langmuir isotherm is represented by following equation [36]

Ceqe=Ceqm+1bqm						(4)

Where qe is the amount adsorbed at equilibrium (mg g-1), Ce is the equilibrium dye solution concentration (mg L-1), qm is Langmuir constant (related to adsorption capacity) (mg g-1) and b is Langmuir constant (related to energy of adsorption) (L mg-1). Fig 6 shows plot of Ce/qe versus Ce, the isotherm parameters are given in table 2.

Fig 6 Langmuir isotherm

3.5.2 Freundlich isotherm

Freundlich isotherm is represented by following equation [36, 37]

logqe=1nlogCe+logkf					(5)

Where kf is adsorption capacity, n is adsorption intensity, Ce is equilibrium dye concentration in solution and qe is equilibrium dye concentration in solid. Fig 7 shows plot of log qe versus log Ce, the isotherm parameters are given in table 2.

Fig 7 Freundlich isotherm

A dimensionless constant called as equilibrium parameter or separation factor RL can be an essential parameter for Langmuir model is given by following equation [36, 38]

RL=11+bC0						(6)

Where b is Langmuir constant (related to energy of adsorption) (L mg-1), C0 is initial dye solution concentration mg L-1. In the present study the value of RL (table 2) lie in between 0 to 1 indicate favourable adsorption.

Table 2 Langmuir and Freundlich isotherm parameter

| Temp (0 K) | Langmuir isotherm parameter |  |  |  | Freundlich isotherm parameter |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | qm (mg g-1) | b (L mg-1) | RL | R2 | n | kf (mg g-1) | R2 |
| 313 | 205.9927 | 0.0149 | 0.7280 | 0.9810 | 1.1798 | 3.3500 | 0.9998 |
| 323 | 199.4389 | 0.0155 | 0.5626 | 0.9620 | 1.1285 | 3.2494 | 0.9999 |
| 333 | 297.9671 | 0.0096 | 0.5809 | 1.0000 | 1.1260 | 3.412 | 0.999 |

3.6 Effect of temperature

In the present study, increase in temperature increases dye removal percentage. Thermodynamic parameter were determined by using following equation.

K0=CsolidCliquid						(7)

Where Csolid is equilibrium solid phase concentration (mg L-1), Cliquid is equilibrium liquid phase concentration (mg L-1) and K0 is equilibrium constant. Gibb’s free energy (ΔG) is represented by following equation

∆G=-RTlnK0						(8)

Where K0 is equilibrium constant, R is gas constant and T is temperature in Kelvin. The Van’t Hoff equation is represented by following equation.

logK0=∆S2.303R-∆H2.303RT					(9)

Fig. 8 represent plot of log K0 versus 1/T, from the slope and intercept of this Van’t Hoff plot the values of ΔH and ΔS were determined and represented in table 3.

Fig 8 log K0 versus 1/T

The value of ΔG is -19.69 to -24.84 (kJ mole-1), ΔH is 14.06 (kJ mole-1) and ΔS is 59.49 (J K-1 mole-1). On the basis of enthalpy ΔH, the adsorption process can be of three type [39]

- Chemical adsorption (80 ˂ ΔH ˂ 450 kJ mole-1)

- electrostatic interaction ( 20 ˂ ΔH ˂ 80 kJ mole-1)

- physical adsorption ( ΔH ˂ 20 kJ mole-1).

The positive value of ΔH indicate an endothermic process. The negative value of ΔG indicate spontaneous and favourable adsorption process. The positive value of ΔS indicate increase in randomness of water molecules surrounding the dye molecules.

Table 3 Thermodynamic parameter of adsorption

| Temp (0 K) | ΔG (kJ mole-1) | ΔH (kJ mole-1) | ΔS (J K-1 mole-1) |
| --- | --- | --- | --- |
| 313 | -19.69 | 14.06 | 59.49 |
| 323 | -22.58 |  |  |
| 333 | -24.84 |  |  |

4 Conclusion

Bio adsorbent prepared from Hyptissuaveolens (VilaytiTulsi) was used to study removal of Rhodamine 6G from aqueous solution under different experimental condition. It has been observed that under optimum condition 48.78 mg g-1 dye can be removed from aqueous solution using the bio adsorbent. The pseudo second order kinetic model was best suited for the present study. Adsorption equilibrium study shows that both Langmuir isotherm and Freundlich isotherm fits for the present study, shows mono layer adsorption process. Thermodynamic study indicate an endothermic, spontaneous adsorption process. This result shows that bio adsorbent prepared from Hyptissuaveolens (VilaytiTulsi) can be used as a low cost adsorbent for the removal of Rhodamine 6G.

5 Acknowledgements

Authors are thankful to University Grants Commission (UGC), New Delhi, for financial support under STRIDE (Component I) (Student Project), authors are also thankful to the Principal, V. P. Mahavidyalaya, Vaijapur for providing laboratory facilities.

Conflict of interest

The authors declare that they have no conflict of interest

6 References

- C. Zaharia, D. Suteu“Textile Organic Dyes – Characteristics, Polluting Effects and Separation/Elimination Procedures from Industrial Effluents – A Critical Overview, Organic Pollutants Ten Years After the Stockholm Convention - Environmental and Analytical Update”, Dr. Tomasz Puzyn (Ed.), ISBN:978-953-307-917-2.Available from: http://www.intechopen.com/books/organic-pollutants-ten-years after-the-stockholm-convention-environmental-and-analytical-update/textile-organic-dyes characteristicspolluting-effects-and-separation-elimination-procedures-from-in. https://doi.org/10.5772/32373, 2012.

- R. Kant, “Textile dyeing industry an environmental hazard” Natural Science, vol. 4, pp. 22-26, 2012. https://doi.org/10.4236/ns.2012.41004

- R. R. Shan, L. G. Yan, Y. M. Yang, K. Yang, S. J. Yu, H. Q. Yu, B. C. Zhu andB. Du,“Highly efficient removal of three red dyes by adsorption onto Mg–Al-layered double hydroxide,” J IndEngChem, Vol. 21, pp.561-568, 2015. https://doi.org/10.1016/j.jiec.2014.03.019

- S. Kumari, G. S. Chauhan andJ. H. Ahn, “Novel cellulose nanowhiskers-based polyurethane foam for rapid and persistent removal of methylene blue from its aqueous solutions,”ChemEng J,vol. 304, pp. 728-736, 2016. https://doi.org/10.1016/j.cej.2016.07.008

- Y. Qi, M. Yang, W. Xu, S. He andY. Men, “Natural polysaccharides-modified graphene oxide for adsorption of organic dyes from aqueous solutions,” J Colloid Interface Sci, vol. 486, pp. 84-96, 2017. https://doi.org/10.1016/j.jcis.2016.09.058

- Cardoso NF, Lima EC, Royer B, Bach, MV, Dotto, GL, Pinto LAA, Calvete T (2012) Comparison of Spirulina platensis microalgae and commercial activated carbon as adsorbents for the removal of Reactive Red 120 dye from aqueous effluents. J Hazard Mater 241−242: 146−153. https://doi.org/10.1016/j.jhazmat.2012.09.

- A.Robab andH.Y.Aziz,“Facile ultrasonic‑assisted preparation of Fe3O4/Ag3VO4 nanocomposites as magnetically recoverable visible‑light‑driven photocatalysts with considerable activity,” J Iran ChemSoc, 2016. https://doi.org/10.1007/s13738-016-1039-z

- N.S.Bhaskar, A.D.Kadam, J.J.Biwal, P.M.Diwate, R.R.Dalbhanjan, D.D.Mahale, S.P.Hinge, B.S.Banerjee, A.V.Mohod and P.R.Gogate,“Removal of Rhodamine 6G from wastewater using solar irradiations in the presence of different additives,”  Desalination and Water Treatment, 2015https://doi.org/10.1080/19443994.2015.1090923.

- D.Lutic, C.C.Pastravanu, I.Cretescu, I.Poulios andC.D.Stan,“Photocatalytic Treatment of Rhodamine 6G inWastewater Using Photoactive ZnO,” International Journal of Photoenergy, 2012. https://doi.org/10.1155/2012/475131

- M.Qamar, M.A.Gondal andZ.H.Yamani,“Removal of Rhodamine 6G induced by laser and catalyzed by Pt/WO3 nanocomposite,” Catalysis Communications,vol. 11, pp.768–772, 2010.  https://doi.org/10.1016/j.catcom.2010.02.012

- Y.M.Zheng, R.F.Yunus, K.G.N.Nanayakkara and J.P.Chen,“Electrochemical Decoloration of Synthetic Wastewater Containing Rhodamine 6G: Behaviors and Mechanism,” IndEngChem Res, vol. 51, pp.5953−5960, 2012. https://doi.org/10.1021/ie2019273.

- M.Chethana, L.G.Sorokhaibam,V.M.Bhandari, S.Raja andV.V.Ranade,“Green Approach to Dye Wastewater Treatment using Biocoagulants,” ACS Sustainable ChemEngvol. 4, 5,pp. 2495-2507, 2016. https://doi.org/10.1021/acssuschemeng.5b01553.

- N.Daneshvar, A.R.Khataee, M.H.Rasoulifard andM.Pourhassan, “Biodegradation of dye solution containing Malachite green: optimization of effective parameters using Taguchi method,” J Hazard Mater, vol.143, pp.214–219, 2007. https://doi.org/10.1016/j.jhazmat.2006.09.016.

- K.S.Bharathi andS.T.Ramesh,“Removal of dyes using agricultural waste as low-cost adsorbents: a review,”Appl Water Sci,vol.3, pp.773–790, 2013. https://doi.org/10.1007/s13201-013-0117-y

- V.K.Gupta, P.J.M.Carrott, M.Ribeiro Carrott and M.L.Suhas,“Low-Cost Adsorbents: Growing Approach to Wastewater Treatment—a Review,”Crit Rev Environ SciTechnolvol. 39, 10, pp. 783-842, 2009.https://doi.org/10.1080/10643380801977610.

- I.Ali andV.K.Gupta, “Advances in water treatment by adsorption technology,” Nat Protocvol.1,6, pp. 2661-7, 2006. https://doi.org/10.1038/nprot.2006.370.

- D.Mohan, K.P.Singh and V.K.Singh,“Wastewater treatment using low cost activated carbons derived from agricultural by products--a case study,” J Hazard Mater vol.152, 3, pp.1045-53, 2008. https://doi.org/10.1016/j.jhazmat.2007.07.079.

- V.L.Meshko, L.Markovska, M.Mincheva and A.E.Rodrigues, (2001) “Adsorption of basic dyes on granular activated carbon and natural zeolite,” Wat Res,vol.35, 14, pp. 3357-3366, 2001. https://doi.org/10.1016/S0043-1354(01)00056-2.

- K.B.Tan, M.Vakili, B.A.Horri, P.E.Poh, A.Z.Abdullah andB.Salamatinia,“Adsorption of dyes by nanomaterials: Recent developments and adsorption mechanisms,” Separation and Purification Technology, vol.150, pp. 229–242, 2015. https://doi.org/10.1016/j.seppur.2015.07.009.

- A.Mishra andT.Mohanty, (2018) “Study of organic pollutant removal capacity for magnetite@ graphene oxide nanocomposites,” Vacuum, 2015.  https://doi.org/10.1016/j.vacuum.2018.08.034.

- F.M.Machado, S.A.Carmalin, E.C.Lima, S.L.P.Dias, L.D.T.Prola, C.Saucier, I.M.Jauris, I.Zanella andS.B.Fagan,“Adsorption of Alizarin Red S Dye by Carbon Nanotubes: An Experimental and Theoretical Investigation,” J PhysChem C,vol.120,pp. 18296−18306, 2016. https://doi.org/10.1021/acs.jpcc.6b03884.

- W.Yin, S.Hao andH.Cao,“Solvothermal synthesis of magnetic CoFe2O4/rGO nanocomposites for highly efficient dye removal in wastewater,” RSC Adv, vol.7, pp. 4062, 2017. https://doi.org/10.1039/c6ra26948f.

- H.Bensalaha, M.F.Bekheetb, S.A.Younssia, M.Ouammoua andA.Gurlob, (2017) “Removal of cationic and anionic textile dyes with Moroccan natural phosphate,” Journal of Environmental Chemical Engineering,vol.5, pp. 2189–2199, 2017. https://doi.org/10.1016/j.jece.2017.04.021

- M.Murugana,  M.J.Ranib, P.Subramaniamc andE.Subramanian,“Use of activated carbon prepared from Prosopisspicigera L. wood (PSLW) plant material for the removal of rhodamine 6G from aqueous solution,” Desalination and Water Treatment, 2014.https://doi.org/10.1080/19443994.2014.986204

- T.Suwunwong, P.Patho, P.Choto andK.Phoungthong, “Enhancement the rhodamine 6G adsorption property on Fe3O4-compositedbiochar derived from rice husk,” Mater Res Express,vol.7, pp. 025511, 2020. https://doi.org/10.1088/2053-1591/ab6b58,

- M.Ahmaruzzaman and V.K.Gupta,“Rice Husk and Its Ash as Low-Cost Adsorbents in Water and Wastewater Treatment,”IndEngChem Res, vol.50, pp.13589–1361, 2011. https://doi.org/10.1021/ie201477c.

- A.M.Barata da Silva, N.O.Serrao, G.G.Celestino, M.L.Takeno, N.T.B.Antunes, S.Iglauer, L.Manzato, F.Auusto de Freitas andP.J.S.Maia,“Removal of rhodamine 6G from synthetic effluents using Clitoriafairchildiana pods as low-cost biosorbent,” Environmental Science and Pollution Research, 2019. https://doi.org/10.1007/s11356-019-07114-6

- F.Deniz,“Adsorption Properties of Low-Cost Biomaterial Derived from Prunusamygdalus L. for Dye Removal from Water,” The Scientific World Journal, 2013. https://doi.org/10.1155/2013/961671.

- A.Alizadeh, A.Parizanganeh, M.R.Yaftian andA.Zamani,“Application of Cellulosic Biomass for Removal of Cationic Dye Rhodamine 6G from Aqueous Solutions,”Int J Waste Resour,vol.6, pp.256, 2016. https://doi.org/10.4172/2252-5211.1000256.

- S.D.Pardeshi, J.P.Sonar, A.M.Zine andS. N. Thore,“Kinetic and thermodynamic study of adsorption of methylene blue and rhodamine B on adsorbent prepared from Hyptissuaveolens (VilaytiTulsi),” J Iran ChemSoc,vol. 10, pp. 1159–1166, 2013. https://doi.org/10.1007/s13738-013-0256-y.

- A.Roy, B.Adhikari and S.B.Majumder,“Equilibrium, Kinetic, and Thermodynamic Studies of Azo Dye Adsorption from Aqueous Solution by Chemically Modified Lignocellulosic Jute Fiber,” IndEngChem Res,vol.52, pp.6502-6512, 2013. https://doi.org/10.1021/ie400236s.

- C.Lei, M.Pi, P.Kuang, Y.Guo and F. Zhang, “Organic dye removal from aqueous solutions by hierarchical calcined Ni-Fe layered double hydroxide: Isotherm, kinetic and mechanism studies,” Journal of Colloid and Interface Science, 2017. http://doi.org/10.1016/j.jcis.2017.02.025.

- H.Lata, V.K.Garg and R. K.Gupta,“Adsorptive removal of basic dye by chemically activated Parthenium biomass: equilibrium and kinetic modelling,”. Desalination,vol.219, pp. 250-261, 2008. https://doi.org/10.1016/j.desal.2007.05.018.

- Y.S.Ho andG.McKay,“A comparison of chemisorptions kinetic models applied to pollutant removal on various sorbents,” Process Safety Environ Prot,vol.76, 4, pp.332–340, 1998. https://doi.org/10.1205/095758298529696

- C.S.Oliveira andC.Airoldi,“Pyridine derivative covalently bonded on chitosan pendant chains for textile dye removal,”Carbohydr.Polym. Vol. 102, pp. 38-46, 2014.https://doi.org/10.1016/j.carbpol.2013.10.075.

- H.N.Tran, S.J.You, B.A.Hosseini and H.P.Chao, “Mistakes and inconsistencies regarding adsorption of contaminants from aqueous solutions: A critical review,” Water Research, 2017.https://doi.org/10.1016/j.watres.2017.04.014.

- A.M.Zine, S.N.Thore, R.P.Pawar, S.D.Pardeshi, N.M.Ligde andJ.P.Sonar,“Adsorption studies of Acid Red 73 on Partheniumhysterophorous L.,” International Journal of Chemical and Physical Sciences vol.7, 4, pp. 13-22, 2018. https://doi.org/10.30731/ijcps.7.4.2018.13-22

- T.W.Weber andR.K.Chakravorti,“Pore and solid diffusion models for fixed-bed adsorbers,”AIChE Journal,vol.20,2, pp.228-238, 1974.https://doi.org/10.1002/aic.690200204.

- F.M.Machado, S.A.Carmalin, E.C.Lima, S.L.P.Dias, L.D.T.Prola, C.Saucier, I.M.Jauris, I.Zanella and S.B.Fagan,“Adsorption of alizarin red S dye by carbon nanaotubes : an experimental and theoretical investigation,” J PhysChem,vol.120, pp.18296-18306, 2016. https://doi.org/10.1021/acs.jpcc.6b03884.