Spectral and Thermal properties of Ho3+   ions doped Zinc Lithium

Alumino Potassiumniobate Borophosphate Glasses

S.L. Meena

Ceramic Laboratory, Department of physics, Jai Narain Vyas University, Jodhpur 342001(Raj.) India

E-mail address:shankardiya7@rediffmail.com

Abstract

Glass of the system: (35-x) P2O5:10ZnO:10Li2O:10Al2O3:10K2O:10Nb2O3:15B2O3:  xHo2O3. (where x=1, 1.5,2 mol %) have been prepared by melt-quenching method. The amorphous nature of the prepared glass samples was confirmed by X-ray diffraction. Optical absorption, Excitation, fluorescence and Thermal spectra were recorded at room temperature for all glass samples. Judd-Ofelt intensity parameters Ωλ (λ=2, 4 and 6) are evaluated from the intensities of various absorption bands of optical absorption spectra. Using these intensity parameters various radiative properties like spontaneous emission probability (A), branching ratio (β), radiative life time (τR) and stimulated emission cross–section ( σp) of various emission lines have been evaluated.

Keywords: ZLAPNBP Glasses, Optical Properties, Judd-Ofelt Theory, Transmittance Properties.

I. Introduction

The rare earth ions doped glasses are used in making up conversion lasers due to their potential applications in variety of fields namely, optical data storage, display technology, undersea transmission and medical diagnostics [1-5].Phosphate glasses are known to be low melting, optical data transmission, detection, laser ,high homogeneity, good corrosion resistance, excellent chemical durability and low glass transition temperature (Tg), better thermal stability, high thermal expansion coefficient, low phonon energy, wide optical transmission region and high refractive index materials, therefore considered to be potential nonlinear materials [6-10]. The high gain density in phosphate glasses is due to high solubility of rare earth ions in phosphate network. These glasses have high luminescence efficiency and they lack thermal lensing effects. When compared with borate and silicate glasses these glasses have distinction optical properties such as large infrared transmission window, high gain density, low up conversion and wide bandwidth emission spectra [11-15]. Recently, phosphate glasses have attained great attention in synthesis, structure and physical properties due to their high density and high dielectric constant [16-18].

The present work reports on the preparation and characterization of rare earth doped heavy metal oxide (HMO) glass systems for lasing materials. I have studied on the Thermal, absorption, Excitation and fluorescence properties of Ho3+ doped zinc lithium alumino potassiumniobate borophosphate glasses. The intensities of the transitions for the rare earth ions have been estimated successfully using the Judd-Ofelt theory, The laser parameters such as radiative probabilities(A),branching ratio (β), radiative life time(τR) and stimulated emission cross section(σp) are evaluated using J.O.intensity parameters( Ωλ, λ=2,4 and 6).

II. Experimental Techniques

Preparation of glasses

The following Ho3+doped borosilicate glass samples (35-x)P2O5:10ZnO:10Li2O:10 Al2O3:10K2O:10Nb2O3:15B2O3: x Ho2O3.  (where x=1,1.5 and 2 mol%)  have been prepared by melt-quenching method. Analytical reagent grade chemical used in the present study consist of P2O5,ZnO, Li2O, Al2O3,K2O,Nb2O3, B2O3 and Ho2O3. They were thoroughly mixed by using an agate pestle mortar. then melted at 10050C by an electrical muffle furnace for 2h., After complete melting, the melts were quickly poured in to a preheated stainless steel mould and annealed at temperature of 2500C for 2h to remove thermal strains and stresses. Every time fine powder of cerium oxide was used for polishing the samples. The glass samples so prepared were of good optical quality and were transparent. The chemical compositions of the glasses with the name of samples are summarized in Table 1.

Table 1.

Chemical composition of the glasses

Sample     	Glass composition (mol %)

ZLAPNBP (UD)         35P2O5:10ZnO:10Li2O:10Al2O3:10K2O:10Nb2O3:15B2O3

ZLAPNBP (HO1)       34P2O5:10ZnO:10Li2O:10Al2O3:10K2O:10Nb2O3:15B2O3:1 Ho2O3

ZLAPNBP (HO1.5)    33.5P2O5:10ZnO:10Li2O:10Al2O3:10K2O:10Nb2O3:15B2O3:1.5Ho2O3

ZLAPNBP (HO2)       33P2O5:10ZnO:10Li2O:10Al2O3:10K2O:10Nb2O3:15B2O3: 2 Ho2O3

ZLAPNBP (UD) -Represents undoped   Zinc Lithium Alumino Potassiumniobate Borophosphate glass specimen.

ZLAPNBP (HO)-Represents Ho3+ doped Zinc Lithium Alumino Potassiumniobate Borophosphate glass specimens.

III. Theory

3.1 Oscillator Strength

The intensity of spectral lines are expressed in terms of oscillator strengths using the relation [19].

fexpt. = 4.318 ×10-9∫ε (ν) d ν                                          (1)

where, ε (ν) is molar absorption coefficient at a given energy ν (cm-1), to be evaluated from Beer–Lambert law.

Under Gaussian Approximation, using Beer–Lambert law, the observed oscillator strengths of the absorption bands have been experimentally calculated [20], using the modified relation:

Pm=4.6 ×10-9×log ×Δυ1/2                                                          (2)

where c is the molar concentration of the absorbing ion per unit volume, I is the optical path length, logI0/I is optical density and Δυ1/2 is half band width.

3.2. Judd-Ofelt Intensity Parameters

According to Judd [21] and Ofelt [22] theory, independently derived expression for the oscillator strength of the induced forced electric dipole transitions between an initial J manifold │4fN (S, L) J> level and the terminal J' manifold │4fN (S',L') J'> is given by:

(3)                                                        Where, the line strength S (J, J') is given by the equation

S (J, J') =e2 ∑ Ωλ<4fN(S, L) J║U (λ) ║4fN (S', L') J'>2                    (4)

λ =2, 4, 6

In the above equation m is the mass of an electron, c is the velocity of light, ν is the wave number of the transition, h is Planck’s constant, n is the refractive index, J and J' are the total angular momentum of the initial and final level respectively, Ωλ (λ=2,4and 6) are known as Judd-Ofelt intensity.

3.3 Radiative Properties

The Ωλ parameters obtained using the absorption spectral results have been used to predict radiative properties such as spontaneous emission probability (A) and radiative life time (τR), and laser parameters like fluorescence branching ratio (βR) and stimulated emission cross section (σp).

The spontaneous emission probability from initial manifold │4fN (S', L') J'> to a final manifold │4fN (S, L) J >| is given by:

A [(S', L') J'; (S, L) J] = 64 π2ν33h2J'+1nn2+229×S(J',J)                       (5)

Where, S (J', J) = e2 [Ω2║U (2) ║2 + Ω4║U (4) ║2 + Ω6║U (6) ║2]

The fluorescence branching ratio for the transitions originating from a specific initial manifold │4fN (S', L') J'> to a final many fold│4fN (S, L) J > is given by

β [(S', L') J'; ( S , L ) J ] =  AS'  L AS' L' J'S  L(6)

S L J

where, the sum is over all terminal manifolds.

The radiative life time is given by

 rad  A[(S', L') J'; (S,L ) ]  = ATotal-1                                       (7)

S L J

where, the sum is over all possible terminal manifolds. The stimulated emission cross -section for a transition from an initial manifold │4fN (S', L') J'> to a final manifold

│4fN (S, L) J >| is expressed as

σpλp=λp48πcn2Δλeff ×AS',L' J';S, LJ                         (8)

where, λp the peak fluorescence wavelength of the emission band and Δλeff is the effective fluorescence line width.

3.4 Nephelauxetic Ratio (β') and Bonding Parameter (b1/2)

The nature of the R-O bond is known by the Nephelauxetic Ratio (β') and Bonding Parameters (b1/2), which are computed by using following formulae [23, 24]. The Nephelauxetic Ratio is given by

β'=νgνa                                                                  (9)

where, νa and νg refer to the energies of the corresponding transition in the glass and free ion, respectively. The value of bonding parameter ( b1/2 ) is given by

b1/2= 1-β'21/2                                                              (10)

IV. Result and Discussion

4.1 XRD Measurement

Figure 1 presents the XRD pattern of the sample contain – P2O5 which is show no

sharp Bragg’s peak, but only a broad diffuse hump around low angle region. This is the clear indication of amorphous nature within the resolution limit of XRD instrument.

Fig. 1 X-ray diffraction pattern of   P2O5:ZnO:Li2O: Al2O3:K2O:Nb2O3:B2O3: Ho2O3

4.2 Thermal Properties

Fig. 2 depicts the DTA thermogram of powdered ZLAPNBP sample show an endothermic peak corresponding to glass transition event followed by an exothermic peak related to crystallization event. The glass transition temperature (Tg), onset crystallization temperature (Tx), crystallization temperature (Tc) were estimated to be 5160C, 5820C and 5950C respectively. From the measured value of Tg, Tx and Tc, the glass stability factor (∆T =Tx-Tg) has been determined to be 660C indicating the good stability of the glass.

Fig. 2. DTA thermogram of powdered ZLAPNBP sample.

Obtained results indicate that by increasing the amount of mol% Ho2O3, the Tg of the samples also increases, the small increase of Tg in these glasses shows that the structure is strongly and progressively modified. The thermal stabilities ΔT of the ZLAPNBP reference glass and Ho+3doped ZLAPNBP glass has been evaluated from their Tg, Tc and Tc values, the results are listed out in Table 2.Hruby’s parameter also calculated by using eq. (11), the greater values of the Hruby’s parameter indicate higher glass forming tendency, the values of Hin our glasses increased with the addition of the Ho2O3.Eqs. (12) and (13) present the GS parameter of Weinberg [25]and Lu and Liu [26], respectively.

H=TX-TgTc-TX                                                                                        (11)

KW=TX-TgTc	     (12)

KLL=TXTg+Tc                                                                                      (13)

Table 2: Thermal parameters determined from the DTA traces of ZLAPNBP (HO) glasses.

| Sample Name | % Sm2O3 | Tg0C | TX0C | TC0C | ΔT | H | KW | KLL |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ZLAPNBP (HO 1.0) | 1 | 516 | 582 | 595 | 66 | 5.076 | 0.1109 | 0.5231 |
| ZLAPNBP (HO 1.5) | 1.5 | 518 | 585 | 598 | 67 | 5.153 | 0.1120 | 0.5242 |
| ZLAPNBP (HO 02) | 2 | 522 | 592 | 605 | 70 | 5.231 | 0.1157 | 0.5253 |

4.3 Absorption Spectrum

The absorption spectra of Ho3+doped ZLAPNBP glass specimens have been presented in Figure 3 in terms of optical density versus wavelength. Twelve  absorption bands have been observed from the ground state 5I8 to excited states 5I5, 5I4, 5F5, 5F4, 5F3, 3K8, 5G6, (5G,3G)5, 5G4, 5G2, 5G3, and3F4 for Ho3+ doped ZLAPNBP glasses.

Fig. (3) Absorption spectrum of Ho3+doped ZLAPNBP HO (01) glass.

The experimental and calculated oscillator strength for Ho3+ ions in ZLAPNBP glasses are given in Table 3.

Table 3: Measured and calculated oscillator strength (Pm×10+6) of Ho3+ions in ZLAPNBPglasses.

| Energy level from 5I8 | Glass ZLAPNBP (HO01) |  | Glass ZLAPNBP (HO1.5) |  | Glass ZLAPNBP (HO02) |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Pexp. | Pcal. | Pexp. | Pcal. | Pexp. | Pcal. |
| 5I5 | 0.53 | 0.24 | 0.48 | 0.24 | 0.45 | 0.24 |
| 5I4 | 0.06 | 0.02 | 0.05 | 0.02 | 0.04 | 0.02 |
| 5F5 | 3.66 | 2.78 | 3.62 | 2.75 | 3.58 | 2.72 |
| 5F4 | 4.60 | 4.29 | 4.56 | 4.25 | 4.52 | 4.22 |
| 5F3 | 1.53 | 2.37 | 1.49 | 2.36 | 1.45 | 2.34 |
| 3K8 | 1.45 | 1.97 | 1.42 | 1.94 | 1.38 | 1.92 |
| 5G6 | 26.68 | 26.63 | 25.28 | 25.26 | 24.78 | 24.78 |
| (5G,3G)5 | 3.82 | 1.72 | 3.76 | 1.68 | 3.72 | 1.67 |
| 5G4 | 0.08 | 0.61 | 0.06 | 0.60 | 0.05 | 0.59 |
| 5G2 | 5.62 | 5.61 | 5.58 | 5.36 | 5.54 | 5.27 |
| 5G3 | 1.50 | 1.40 | 1.46 | 1.37 | 1.42 | 1.35 |
| 3F4 | 1.38 | 4.20 | 1.32 | 4.12 | 1.27 | 4.08 |
| r.m.s. deviation | ±1.1031 |  | ±1.0975 |  | ±1.0977 |  |

Computed values of F2, Lande′ parameter (ξ4f), Nephlauxetic ratio (β') and bonding

parameter (b1/2) for Ho3+ ions in ZLAPNBP glass specimen are given in Table 4.

Table 4: F2, ξ4f, β' and b1/2 parameters for Holmium doped glass specimen.

| Glass Specimen | F2 | ξ4f | β' | b1/2 |
| --- | --- | --- | --- | --- |
| Ho3+ | 358.82 | 1258.16 | 0.9337 | 0.1821 |

In the Zinc Lithium Alumino Potassiumniobate Borophosphate glasses (ZLAPNBP) Ω2, Ω4 and Ω6 parameters decrease with the increase of x from 1 to 2 mol%. The order of magnitude of Judd-Ofelt intensity parameters is Ω2>Ω6> Ω4 for all the glass specimens. The spectroscopic quality factor (Ω4 /Ω6) related with the rigidity of the glass system has been found to lie between 0.6181 and 0.6294 in the present glasses.

The values of Judd-Ofelt intensity parameters are given in Table 5.

Table 5: Judd-Ofelt intensity parameters for Ho3+ doped ZLAPNBP glass specimens.

| Glass Specimen | Ω2(pm2) | Ω4(pm2) | Ω6(pm2) | Ω4 /Ω6 | Ref. |
| --- | --- | --- | --- | --- | --- |
| ZLAPNBP (HO01) | 6.576 | 1.369 | 2.175 | 0.6294 | [P.W.] |
| ZLAPNBP (HO1.5) | 6.186 | 1.338 | 2.160 | 0.6194 | [P.W.] |
| ZLAPNBP (HO02) | 6.051 | 1.324 | 2.142 | 0.6181 | [P.W.] |

4.4 Excitation Spectrum

The Excitation spectra of Ho3+doped ZLAPNBP glass specimens have been presented in Figure 4 in terms of Excitation Intensity versus wavelength. The excitation spectrum was recorded in the spectral region 325–525 nm fluorescence at 545nm having different excitation band centered at 350,419, 452, 472and 485 nm are attributed to the 5G3, (5G, 3G)5,   5G6, 3K8 and 5F3 transitions, respectively. The highest absorption level is 5G6 and is at 452nm.So this is to be chosen for excitation wavelength.

Fig. (4) Excitation spectrum of doped with Ho3+  ZLAPNBP glasses.

4.5 Fluorescence Spectrum

The fluorescence spectrum of Ho3+doped in zinc lithium alumino potassiumniobate borophosphate glass is shown in Figure 5. There are five broad bands observed in the Fluorescence spectrum of Ho3+doped zinc lithium alumino potassiumniobate glass. The wavelengths of these bands along with their assignments are given in Table 6. The peak with maximum emission intensity appears at 555 nm and corresponds to the (5F4→5I8) transition.

Fig. (5). Fluorescence spectrum of doped with Ho3+ ZLAPNBP glasses

Table6: Emission peak wave lengths (λp),radiative transition probability (Arad),branching ratio (β),stimulated emission cross-section( σp) and radiative life time( τR ) for various transitions in Ho3+ doped ZLAPNBP glasses.

| Transition |  | ZLAPNBP (HO 01) |  |  |  | ZLAPNBP (HO 1.5) |  |  |  | ZLAPNBP ( HO 02) |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | λmax (nm) | Arad(s-1) | β | σp (10-20 cm2) | τR(μs) | Arad(s-1) | β | σp (10-20 cm2) | τR (μs) | Arad(s-1) | β | σp (10-20 cm2) | τR (10-20 cm2) |
| 5F3→5I8 | 435 | 4086.30 | 0.2641 | 0.5233 | 6464.10 | 4069.01 | 0.2648 | 0.509 | 6506.51 | 4040.35 | 0.2646 | 0.490 | 6549.07 |
| 5F4→5I8 | 501 | 6517.41 | 0.4213 | 1.146 |  | 6467.20 | 0.4208 | 1.124 |  | 6428.04 | 0.4210 | 1.083 |  |
| 5S2→5I8 | 555 | 1706.85 | 0.1103 | 0.396 |  | 1698.46 | 0.1105 | 0.389 |  | 1686.75 | 0.1105 | 0.381 |  |
| 5F5→5I8 | 652 | 1864.64 | 0.1205 | 0.710 |  | 1846.06 | 0.1201 | 0.693 |  | 1833.92 | 0.1201 | 0.675 |  |
| 5S2→5I7 | 761 | 1294.87 | 0.08370 | 0.948 |  | 1288.50 | 0.08384 | 0.934 |  | 1280.31 | 0.08385 | 0.910 |  |
| V. Conclusion In the present study, the glass samples of composition(35-x)P2O5:10ZnO:10Li2O:10 Al2O3:10K2O:10Nb2O3:15B2O3:xHo2O3. (where x =1, 1.5and 2mol %) have been prepared by melt-quenching method. The value of stimulated emission cross-section (σp) is found to be maximum for the transition (5F4→5I8) for glass ZLAPNBP (HO 01), suggesting that glass ZLAPNBP (HO 01) is better compared to the other two glass systems ZLAPNBP (HO1.5) and ZLAPNBP (HO02). The greater values of the Hruby’s parameter indicate higher glass forming tendency. References [1]. Monisha, M, Nancy, Ashwitha, Souza, D., legde,Vinod, Prabhu, N. S. and Sayyed, M.I. (2020).Dy3+ doped SiO2- B2O3-Al2O3-NaF-ZnF2 glasses : An exploration of optical and gamma radiation shielding features, Current Applied Physics 20(11), 1207-1210. [2]. Prabhu, N. S., Hegde,V., Sayyed, M.I. , Agar, O. and Kamath, S. D. (2019). Investigations on structural and radiation shielding properties of Er3+ doped zinc bismuth borate glasses, Materials chemistry and physics, 230,267-276. [3]. Patwari, R., Eraiah, B.(2019).Optical and Plasmonic properties of Er3+ and silver co-doped borate nano- composite glasses, Materials Research Express 6(11),116218. [4]. Sienkiewicz, P., Palkowslea, A., pietr-zyeki, M., Romanczunk, P., Zmojda, J., koxhanowicz, M. and Dorosz, D. (2014).Multicolour up conversion emission in tellurite glasses co-doped with rare earth ions for white LED applications, Photonics Applications in Astronomy, Communications, Industry and High Energy physics experimens. [5]. Liggins, K., Edwards,V. M. and Reddy, B. R. (2017). White light Emission characteristics of rare earth ion doped sodium borate glass,” Optical Components and materials. [6]. El Maaref, A.A., Badr,S., Shaaban, Kh.S., Abdel Wahab, E.A. and Elokr, M.M.(2019). Optical properties and radiative rates of Nd3+ doped zinc- sodium phosphate Glasses,” Journal of rare Earth, 37, 253-259. [7]. Ratnakaram,V. C., Reddy Prasad, V., Babu, S. and Kumar,V. V. R. K.(2016). “Luminescence performance of Eu3+ doped lead free zinc phosphate glasses for red emission,” Bulletin of Materials Science 39, 1065-1072. [8]. Babu,S. S., Babu, P., Jayasankar, C.K., Sievers, W. and Wortmann, G.(2007).Optical absorption and photolumibescence studies of Eu3+ doped phosphate and flurophosphate glasses, Journal of luminescence,126,109-120. [9]. Venkatramu, V., Vijaya, R., Luis, S.F., Babu, P., Jayasankar, C.K., Lavin, V. and Dhareshwar, L.J.(2011). Optical properties of Yb3+ doped phosphate laser glasses,” Journal of Alloys and Compounds,509,5084-5089. [10].Christopher, A.G., Kalnnis, H., Ebendorff, H., Nigel A Spooner and Tanya M, Marno,(2011).Optically stimulated luminescence in fluoride phosphate glass for radiation dosimetry, Journal of the American Ceramic Society ,94(2),474-477. [11].Wojciench, A., Pisarski Lidia, Zur, Tomasz, Goryczka, Marta, S. and Piesarska, Joanna (2014). Structure and Spectroscopy of rare earth doped lead phosphate glasses.(Eu,Tb, Dy, Er), Journal of Alloys and Compound 587, 90-98(2014). [12]. Seshadri, M., Radha, M., Barbosa, C., Cordeiro, C.M.B. and Ratnaka, Y.C.(2015).Effect of ZnO on spectroscopic properties of Sm3+ doped zinc phosphate glasses, Physica B: Condensed matter 459, 79-87. [13]. Marzouk,M.A., ElBatel, H. A., Hamdy, Y.M. and Ezz-Eldin, F. M.(2019).Collective Optical, FTIR and Photoluminescence Spectra of CeO2 and Sm2O3 Doped Na2O-ZnO-P2O5 Glasses, International Journal of Optics. [14]. Mitra,S. and Jana, S.(2015). Intense orange emission in Pr3+ doped lead phosphate glass, Journal of physics and chemistry of solids 85,245-253. [15]. Amlah S., Azmi,M., Sahar, M.R., Ghoshal, S.K. and Arifin, R.(2015).Modification of structural and physical properties of samarium doped zinc phosphate glasses due to the inclusion of nickel oxide nanoparticles,” Journal of Non crystalline Solids 411,53-58. [16]. Chen,Y., Chen,G.H., Liu,X.Y. and Yang, T.(2018).Enhanced up – conversion luminescence and optical thermometry characteristics of Er3+/ Yb3+ co-doped transparent phosphate Glass Ceremics, Journal of luminescence 195,314-320. [17].Liyu Hao, Manting Pei, Tie Yang, Chengguo Ming(2020).Double sensitivity temperature sensor based on excitation intensity ratio of Eu3+ doped phosphate glass ceramic, Optik 204,164188. [18]. Dutebo, M. T., Shashikala, H.D.(2020).Influence of (Er3+, La3+, Ce4+) additions on physical and optical properties of 50 CaO- 50 P2O5 glasses, Physica B: Condensed Matter 597, 412358. [19]. Gorller-Walrand, C. and Binnemans, K. (1988) Spectral Intensities of f-f Transition. In: Gshneidner Jr., K.A. and Eyring,L., Eds., Handbook on the Physics and Chemistry of Rare Earths, Vol. 25, Chap. 167, North-Holland, Amsterdam, 101. [20].Sharma, Y.K., Surana, S.S.L. and Singh, R.K. (2009). Spectroscopic Investigations and Luminescence Spectra of Sm3+ Doped Soda Lime Silicate Glasses. Journal of Rare Earths, 27, 773. [21].Judd, B.R. (1962). Optical Absorption Intensities of Rare Earth Ions.Physical Review, 127, 750. [22].Ofelt, G.S. (1962). Intensities of Crystal Spectra of Rare Earth Ions. The Journal of Chemical Physics, 37, 511. [23].Sinha, S.P. (1983).Systematics and properties of lanthanides, Reidel, Dordrecht. [24]. Krupke,W.F.(1974).Induced- emission cross-section in neodymium laser glasses. IEEE J. Quantum electron QE-10,450-457. [25]. Weinberg,M.C.(1994). Experimental test of surface nucleated crystal growth model in lithiumdiborate glass, Phys. Chem. Glasses 35, 119. [26]. Lu, Z.P. and Liu, C.T.(2003).Glass Formation Criterion for Various Glass-Forming Systems Phys. Rev. Lett. 91,11550 . [5]Damodaraiah [6].V.N. Rai, B.N. Raja Sekhar, S. Kher, S.K. Deb, “Effect of gamma ray irradiation on optical properties of Nd doped phosphate glass,” Journal of luminescence,” 582-586(2010). [7].SNS Yaacob, MR Sahar, ES Sazali, Zahra Ashur Mahraz, K Sulhadi, Zahara Ashur Mahraz, K Sulhadi,(2018). “Comprehensive study on compositional modification of Tb3+ doped Zinc phosphate Glass,” Solid State Sciences 81,51-57. [4].V.N. Rai, B.N. Raja Sekhar, P. Tiwari, R.J. Kshirsagar, S.K. Deb, “Spectroscopic studies of gama irradiated Nd doped phosphate Glasses,” Journal of Non- crystalline soilds, 3757-3764(2011). [1].A.A. El Maaref, Shiaa Badr, Kh.S. Shaaban, E.A. Abdel Wahab, M.M. Elokr, “Optical properties and radiative rates of Nd3+ doped zinc- sodium phosphate Glasses,” Journal of rare Earth, 37, 253-259(2019). [2]. V C Ratnakaram, V Reddy Prasad, S Babu, V V Ravi kanth kumar, “Luminescence performance of Eu3+ doped lead free zinc phosphate glasses for red emission,” Bulletin of Materials Science 39, 1065-1072(2016). [3]. S. Surendra Babu, P. Babu, C.K. Jayasankar, W. Sievers, G. Wortmann, “Optical absorption and photolumibescence studies of Eu3+ doped phosphate and flurophosphate glasses,” Journal of luminescence,126,109-120(2007). [4]. V.Venkatramu, R. Vijaya, S.F. Luis, P.Babu, C.K. Jayasankar, V. Lavin, L.J. Dhareshwar, “Optical properties of Yb3+ doped phosphate laser glasses,” Journal of Alloys and Compounds,509,5084-5089(2011). [5].Christopher AG Kalnnis, Heike Ebendorff H., Nigel A Spooner, Tanya M Marno, “Optically stimulated luminescence in fluoride phosphate glass for radiation dosimetry,” Journal of the American Ceramic Society ,94(2),474-477(2011). [6].Liyu Hao, Manting Pei, Tie Yang, Chengguo Ming, “Double sensitivity temperature sensor based on excitation intensity ratio of Eu3+ doped phosphate glass ceramic,” Optik 204,164188(2020). [7].Mathewos Tulore Dutebo, HD Shashikala, “Influence of (Er3+, La3+, Ce4+) additions on physical and optical properties of 50 CaO- 50 P2O5 glasses,” Physica B: Condensed Matter 597, 412358(2020). [8].M.A. Marzouk, H. A. ElBatel, Y.M. Hamdy, F. M. Ezz-Eldin, “Collective Optical, FTIR and Photoluminescence Spectra of CeO2 and Sm2O3 Doped Na2O-ZnO-P2O5 Glasses,” International Journal of Optics(2019). [9].Subrata Mitra, Samar Jana, “ Intense orange emission in Pr3+ doped lead phosphate glass,” Journal of physics and chemistry of solids 85,245-253(2015). [10]. Siti Amlah M Azmi, MR Sahar, SK Ghoshal, R Arifin, “Modification of structural and physical properties of samarium doped zinc phosphate glasses due to the inclusion of nickel oxide nanoparticles,” Journal of Non crystalline Solids 411,53-58(2015). [11].Y Chen, GH Chen, XY Liu, T Yang, “Enhanced up – conversion luminescence and optical thermometry characteristics of Er3+/ Yb3+ co-doped transparent phosphate Glass Ceremics,” Journal of luminescence 195,314-320(2018). [12].Wojciench A Pisarski Lidia Zur, Tomasz Goryczka, Marta sottys, Joanna Piesarska, “Structure and Spectroscopy of rare earth doped lead phosphate glasses.(Eu,Tb, Dy, Er),” Journal of Alloys and Compound 587, 90-98(2014). M Seshadri, M Radha, C Barbosa, CMB Cordeiro, YC Ratnaka, “Effect of ZnO on spectroscopic properties of Sm(3+) doped zinc phosphate glasses,” Physica B: Condensed matter 459, 79-87 (2015). [5]Damodaraiah, S., Prasad, V. R., Babu, S. and Ratnakaram, Y. C. (2017). “Structural and luminescence properties of Dy3+ doped bismuth phosphate glasses for greenish yellow light applications”. Optical Materials, 67, 14-24. [13]. Gorller-Walrand, C. and Binnemans, K. (1988) Spectral Intensities of f-f Transition. In: Gshneidner Jr., K.A. and Eyring,L., Eds., Handbook on the Physics and Chemistry of Rare Earths, Vol. 25, Chap. 167, North-Holland, Amsterdam, 101-264. [14]. Sharma, Y.K., Surana, S.S.L. and Singh, R.K. (2009) Spectroscopic Investigations and Luminescence Spectra of Sm3+ Doped Soda Lime Silicate Glasses. Journal of Rare Earths, 27, 773. [15]. Judd, B.R. (1962). Optical Absorption Intensities of Rare Earth Ions. Physical Review, 127, 750. [16]. Ofelt, G.S. (1962). Intensities of Crystal Spectra of Rare Earth Ions. The Journal of Chemical Physics, 37, 511. [17].Sinha, S.P. (1983).Systematics and properties of lanthanides, Reidel, Dordrecht. [18].Krupke, W.F. (1974).IEEE J.Quantum Electron QE, 10,450. # [19].Rajikumar, P. R.,Vasudevan, P.,Karthika, S., Georg, J.(2010). Structural and spectroscopic characterization of Ho3+ in sol-gel silica glasses, J.Opt.and Advan. Materials, 12, 1065-1070. [20]. Boyer, J.C., Vertone, F., Capobianco, J.A., Speghini, A., Bettinelli, M. (2003). J. Appl. Phys. 93, 9461. |  |  |  |  |  |  |  |  |  |  |  |  |  |