Adsorptive removal of Amido black from aqueous solution using low cost adsorbent: Kinetic and isotherm study

A. S. SALUNKE1. N. N. GUND1.B. M. MARMAT1. J. P. SONAR 1. S. A. DOKHE1.

A. M. ZINE 1.  S. N. THORE1. S. D. PARDESHI1*.

1 Department of Chemistry, Vinayakrao Patil Mahavidyalaya, Vaijapur, Maharashtra 423 701, India.

* Orcid ID orcid.org/0000-0001-8794-5629

*Corresponding Author E-Mail: sandeeppardeshi007@gmail.com

Abstract

In the present study the removal of Amido black 10B from aqueous solution by adsorption on adsorbent prepared from Hyptissuaveolens (vilaytitulsi) is studied. The effect of pH, contact time, dye concentration, adsorbent dose and temperature was investigated. The isotherm study shows that Langmuir isotherm was best fitted for present work. The adsorption follows pseudo-second order kinetic. An increase in temperature decreases the dye removal.

Keywords: Amido black dye, Adsorption, Hyptissuaveolens, VilaytiTulsi

1. Introduction

Water is one of the essential parts of human life; due industrialisation and urbanization water pollution becomes a major issue. Large amount of organic pollutant such as dyes, phenols etc. are present in industrial effluents and cause contamination of water. Dyes are one the important organic pollutant present in industrial effluents [1]. Dyes are widely used in textile and leather industries, the effluent of these industries always contain some amount of dyes. Azo dyes are, widely used in textile industries, characterised by –N=N- bond [2]. Amido black 10B is a azo dye used to colour cotton, wool, nylon, rayon etc. [3], it may cause skin and eye irritation, serious damage to respiratory system [4]. Many methods are used to remove dyes from water such as photo catalytic decolourisation [5], microbial degradation [6], precipitation [7, 8] etc. out these technique adsorption is most commonly used technique for dye removal from aqueous solution [9]. Activated carbon is the most widely used adsorbent [10] but cellulose based adsorbent, due to low cost and wide availability, attracted the researcher for their application in dye removal [11]. Various low cost bio adsorbents are reported such as Palm Shell Powder [9], jute fibre[11], rice husk [12], neem saw dust [13] etc. the literature reveals the application of various adsorbents [14,15].

In the present study the adsorptive capacity of adsorbent prepared Hyptissuaveolens was investigated for the azo dye Amido black 10B. The adsorption efficiency of the adsorbent prepared was studied by applying various parameters such as temperature, dye concentration, contact time and adsorbent dose.

2. Experimental

2.1Preparation of Adsorbent

Fully grown plants of Hyptissuaveolens (VilaytiTulsi) were collected from places nearby vaijapur city and cut into small pieces, washed with distilled water, dried under shed. The adsorbent was prepared as per the procedure mentioned in our earlier publication [16].

2.2 Preparation of dye solution

Amido black10 B (AB), was purchased from Loba Chem Pvt. Ltd. Indiawas used for present study. The molecular formula is C22H14N6Na2O9S2, and the maximum absorbance observed at wavelength 618 nm.   A stock solution of 500 mg L-1 was prepared by dissolving accurately weigh dye quantity in double distilled water. Dilution with double distilled was carried out to get desired experimental concentration.

2.3 Adsorption Studies

50mL sorbet solution of predetermined pH and dye concentration was taken in 250 mL stoppered conical flask, 100mG adsorbent was added,and the solution was mechanically stirred. Requisite amount of solution was removed at predetermined time and centrifuge at 2,000 rpm to separate adsorbent from dye solution. 0.1 M HCl and 0.1 M NaOh was used to adjust the initial pH. The sorbet amount remain unadsorbed was determine by measuring absorption of supernatant solution using Elico double beam spectrophotometer SL-210.the adsorption capacity was determined using the Langmuir and Freundlich isotherm.

Equation 1 was used to find the solid phase dye concentration

qt=C0-CtVW						(1)

Where Co is initial dye concentration and Ct is dye concentration at time t in mg L-1, V is volume of solution in L qt is adsorption amount at time t, and W is weight of adsorbent in g.

3 Results and Discussion

3.1 Effect of pH

The adsorption of ionized dyes on the surface of adsorbent is mainly depend on initial pH rather than final [17]. 0.1 g adsorbent was shaken for 30 min with 50 mL solution of 50mg L-1 dye concentration. It has been observed that the adsorption is not much affected if the pH is varied from 2 to 4, further increase in pH decreases the dye removal. Lower pH favours the adsorption may be due to higher electrostatic attraction between adsorbent surface and dye [17]. As shown in the Fig.1, pH 4 is considered as optimum pH for further studies.

Fig 1. Effect of pH on dye removal

Fig. 2 Effect of pH on dye removal

3.2 Effect of Adsorbent dose

Amount of adsorbent is one of the main parameter which affect the adsorption, 50mL dye solution with 50 mg L-1 dye concentration was stirred with predetermined amount of adsorbent (0.05 to 0.3 g). The percentage of dye removal increases with increase in amount of adsorbent from 70.94 to 92.50 % but the unit adsorption was decline from 35.47 mg g-1 to 7.70 mg g-1with increase in adsorbent dose amount as shown in Fig 3 and Fig 4 this may be due to increase in the number of vacant adsorption site with increase the amount of adsorbent dose [18].

Fig. 3 Effect of Adsorbent dose

Fig. 4 Effect of Adsorbent dose

3.3 Effect of dye concentration

50 mL solution of optimum pH and predetermined concentration (25 mg L-1 to 100 mg L-1) was stirred with 0.1 g adsorbent, the results are shown in Fig. 5. Initially there was large number of adsorption site are available due which the initial rate of adsorption was fast [19]. The percentage removal of AB decreases with increase in solution concentration but the unit adsorption increases.

Fig. 5 Effect of initial dye concentration on adsorption

3.4 Adsorption dynamics

3.4.1 The pseudo first order kinetic model

The pseudo first order kinetic model expression is given by Lagergren [20] as follows

logqe-qt=logqe-k1t2.303					(2)

Where qt and qe are amount of dye adsorbed at time t and equilibrium, respectively k1 is the rate constant..

3.4.2 The pseudo second order kinetic model

The pseudo second order Lagergren equation is expressed as [21]

tqt=1qe2k2+tqt						(3)

The Fig.4 shows Plot of t/qtversus t. Values of equilibrium adsorption capacity (qe) and second order rate constant (k2) were determined from the slopes and intercepts and represented in table 1. From the table number 1 it has been observed that the present adsorption process was depend on both adsorbent and dye concentration, thus follows pseudo second order kinetic model

Fig. 6 The pseudo second order kinetic

3.4.2 The intra particle diffusion model

The intra particle diffusion model is expresses as [22]

qt=t21kp     						(4)

Where qt is adsorption capacity and kp is intra particle diffusion constant, plot of qt versus t1/2 give the value of kp, as from the R2 value for intra particle diffusion model, the present study does not fits in it

Table 1 Rate constants for pseudo first-order, pseudo second-order adsorption and intra particle diffusion model

| Conc. C0 (mg L-1) | pseudo first-order |  |  | pseudo second-order |  |  | Intra particle diffusion |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | qe (mg g-1) | K1 (min-1) | R2 | qe (mg g-1) | K2 (min-1) | R2 | Kp (mg/(g min1/2) | R2 |
| 50 | 2.1832 | 0.04767 | 0.9244 | 10.5374 | 0.04722 | 0.999 | 0.1904 | 0.961 |
| 75 | 1.7290 | 0.05365 | 0.968 | 24.3902 | 0.2425 | 1.00 | 0.0083 | 0.9591 |
| 100 | 5.2107 | 0.03915 | 0.9612 | 36.3636 | 0.5817 | 1.00 | 0.0125 | 0.9771 |
| 125 | 13.7499 | 0.0244 | 0.9124 | 48.7804 | 1.4009 | 1.00 | 0.0261 | 0.9125 |

3.5 Adsorption equilibrium study

Two isotherm, Langmuir isotherm and Freundlich isotherm was used for present study.

3.5.1 Langmuir isotherm

Langmuir isotherm is represented by following equation [23]

Ceqe=Ceqm+1bqm						(4)

Where Ce is the equilibrium dye solution concentration (mg L-1),qm is Langmuir constant (related to adsorption capacity) (mg g-1), b is Langmuir constant (related to energy of adsorption) (L mg-1)and qe is the amount adsorbed at equilibrium (mg g-1).

3.5.2 Freundlich isotherm

Freundlich isotherm is represented by following equation [23]

logqe=1nlogCe+logkf					(5)

Where n is adsorption intensity, kf is adsorption capacity, qe is equilibrium dye concentration in solid and Ce is equilibrium dye concentration in solution. The isotherm parameters are given in table 2.

Table 2 Langmuir and Freundlich isotherm parameter

| Temp (0 K) | Langmuir isotherm parameter |  |  | Freundlich isotherm parameter |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | qm (mg g-1) | b (L mg-1)*103 | R2 | n | kf (mg g-1) | R2 |
| 313 | 24.69 | 16.63 | 1 | 151.51 | 13.77 | 0.9977 |
| 323 | 24.44 | 17.85 | 1 | 158.73 | 24.59 | 0.9973 |
| 333 | 24.09 | 20.00 | 1 | 166.66 | 24.60 | 0.9972 |

4 Conclusion

Adsorptive removal of Amido black 10B was studied on Bio adsorbent prepared from Hyptissuaveolens (VilaytiTulsi). The present study follows the pseudo second order kinetic model and the Langmuir isotherm model was most applicable to present study. The low pH and low temperature favours the adsoption of Amido black 10B from aqueous solution. The adsorbent prepared from Hyptissuaveolens (VilaytiTulsi) can be used as a low cost adsorbent for the removal of Amido black 10B.

5 Acknowledgements

Authors are thankful to The Principal, Vinayakrao Patil Mahavidyalaya, Vaijapur and University Grants Commission (UGC), New Delhi, for providing financial assistance under STRIDE (Component I). Authors are also thankful to the Principal, Vinayakrao Patil Mahavidyalaya, Vaijapur for providing laboratory facilities.

Compliance with ethical standards

Conflict of interest

The authors declare that they have no conflict of interest

- References

- L. Ali1, H. Alhassani, N. Karuvantevida, M. A. Rauf and S. S. Ashraf, “Efficient Aerobic Degradation of Various Azo   Dyes by a Sphingomonas sp Isolated from Petroleum Sludge”,  Journal of Bioremediation & Biodegradation, 5,3, (2014) https://doi.org/10.4172/2155-6199.1000223.

- W. Jia, D. Lu, S. Shuang, J. Yang and C. Dong, “Facile Synthesis of Chitosan Modified Fe3O4 Magnetic Nanoparticles for Azo Dye Amido Black 10B Adsorption”, Journal of Nano Research, 49, 149-162.

- R. Kaurand H.  Kaur, “Adsorptive Removal of Amido Black 10B from AqueousSolution using Stem Carbon of Ricinuscommunisas Adsorbent” Asian Journal of Chemistry,  31, 5 1071-1076 (2019),https://doi.org/10.14233/ajchem.2019.21813

- A. Mittal, V. Thakur and V. Gajbe, “Adsorptive removal of toxic azo dye Amido Black 10B by hen feather” Environ. Sci. Pollut. Res., https://doi.org/10.1007/s11356-012-0843-y

- M.A. Gondala, X.F. Chang and Z.H. Yamani, “UV-light induced photocatalytic decolorization of Rhodamine 6G molecules over BiOCl from aqueous solution” Chemical Engineering Journal, 165, 250–257, (2010). https://doi.org/10.1016/j.cej.2010.09.025

- R. Kant, “Textile dyeing industry an environmental hazard” Natural Science, 4,22-26, (2012), http://dx.doi.org/10.4236/ns.2012.41004

- A.K. Verma, R.R. Dash and P. Bhunia, A review on chemical coagulation/flocculation technologies for removal of colour from textile wastewaters, J. Environ. Manage. 93 (2012) 154–168.

- M. Murugan, M. J. Rani, P. Subramaniam and E. Subramanian, “Use of activated carbon prepared from Prosopis spicigera L. wood (PSLW) plant material for the removal of rhodamine 6G from aqueous solution” Desalination and Water Treatment, http://dx.doi.org/10.1080/19443994.2014.986204

- G.Sreelatha and P.Padmaja, “Study of Removal of Cationic Dyes using Palm Shell Powder as Adsorbent” Journal of environmental protection science, 2, 63 – 71, (2008).

- C. He and X. Hu, “Anionic Dye Adsorption on Chemically Modified Ordered Mesoporous Carbons” Industrial & Engineering Chemistry Research, 50, 14070-14083, (2011), http://dx.doi.org/10.1021/ie201469p

- A. Roy, B. Adhikari, and S. B. Majumder, “Equilibrium, Kinetic, and Thermodynamic Studies of Azo Dye Adsorption from Aqueous Solution by Chemically Modified Lignocellulosic Jute Fiber” Industrial & Engineering Chemistry Research, 52,6502-6512, (2013), http://dx.doi.org/10.1021/ie400236s

- M. Ahmaruzzaman and V. K. Gupta, “Rice Husk and Its Ash as Low-Cost Adsorbents in Water and Wastewater Treatment” Industrial & Engineering Chemistry Research, 50, 13589-13613, (2011), http://dx.doi.org/10.1021/ie201477c

- S.D. Khattria and M.K. Singh, “Removal of malachite green from dye wastewater using neem sawdust by adsorption” Journal of Hazardous Materials, 167, 1089–1094,(2009). https://doi.org/10.1016/j.jhazmat.2009.01.101

- K. S. Bharathi  and S. T. Ramesh, “Removal of dyes using agricultural waste as low-cost adsorbents: a review” Applied Water Science,  3, 773–790, (2013) https://doi.org/10.1007/s13201-013-0117-y

- G. Crini, “Non-conventional low-cost adsorbents for dye removal: A review” Bioresource Technology, 97, 1061–1085, (2006), https://doi.org/10.1016/j.biortech.2005.05.001

- S. D. Pardeshi,J. P.Sonar, A. M. Zine and S. N. Thore, “Kinetic and thermodynamic study of adsorption of methylene blue and rhodamine B on adsorbent prepared from Hyptissuaveolens (VilaytiTulsi)”. Journal of the Iranian Chemical Society, 10, 1159–1166, (2013). https://doi.org/10.1007/s13738-013-0256-y

- R. Kaurand H.  Kaur, “Adsorptive Removal of Amido Black 10B from AqueousSolution using Stem Carbon of Ricinuscommunisas Adsorbent” Asian Journal of Chemistry,  31, 5 1071-1076 (2019),https://doi.org/10.14233/ajchem.2019.21813

- G.Sreelathaand  P. Padmaja, “Study of Removal of Cationic Dyes using Palm Shell Powder as Adsorbent”  Journal of Environmental Protection Science2, 63 – 71(2008).

- S.D. Khattria and M.K. Singh, “Removal of malachite green from dye wastewater using neem sawdustby adsorption” Journal of Hazardous Materials, 167, 1089–1094,(2009). https://doi.org/10.1016/j.jhazmat.2009.01.101

- N. N. Gund , B. M. Marmat , A. S. Salunke , J. P. Sonar , S. A. Dokhe ,A. M. Zine , S. N. Thore  and S. D. Pardeshi, “Removal of Rhodamine 6G from Aqueous Solution by Adsorption on Bio Adsorbent Prepared from HyptisSuaveolens (VilaytiTulsi): Kinetic,  Equilibrium and Thermodynamic Study”, International Journal of Chemical and Physical Sciences, 10, 2 , (2021), https://doi.org/10.30731/ijcps.10.3.2021.1-9

- A. M. Zine, S. N. Thore , R. P. Pawar ,S. D.  Pardeshi, N. M. Ligdeand J. P. Sonar, “Adsorption studies of Acid Red 73 on Partheniumhysterophorous L.”  International Journal of Chemical and Physical Sciences 7, 4: 13-22, (2018). https://doi.org/10.30731/ijcps.7.4.2018.13-22

- H.Bensalaha,, M. F. Bekheetb, S. A.Younssia, M.Ouammoua and A.Gurlob, “Removal of cationic and anionic textile dyes with Moroccan naturalphosphate”,Journal of Environmental Chemical Engineering 5, 2189–2199, (2017). http://dx.doi.org/10.1016/j.jece.2017.04.021

- H.Lata, V.K. Gargand and R.K. Gupta, “Adsorptive removal of basic dye by chemically activatedParthenium biomass: equilibrium and kinetic modelling” Desalination, 219, 250–261, (2008). http://dx.doi.org/10.1016/j.desal.2007.05.018