Spectral and Raman Analysis of Nd3+ Doped Zinc Lithium Sodalime Cadmium Borosilicate Glasses

S.L.Meena

Ceremic Laboratory, Department of physics, Jai Narain Vyas University, Jodhpur 342001(Raj.) India

E-mail address:shankardiya7@rediffmail.com

Abstract

Glass of the system: (35-x) SiO2:10ZnO:10Li2O:10CaO:10Na2O:10CdO:15B2O3:  xNd2O3. (where x=1, 1.5,2 mol %) have been prepared by melt-quenching method. The amorphous nature of the glasses was confirmed by X-ray diffraction studies. Optical absorption, Excitation, fluorescence and Raman spectra have been recorded at room temperature for all glass samples.Slater-Condon parameters Fk (k=2, 4, 6), Lande’s parameter ξ4f and Racah parameters Ek (k=1, 2, 3) have been computed. Using these parameters energies and intensities of these bands has been calculated. Judd-Ofelt intensity parameters Ωλ (λ=2, 4, 6) are evaluated from the intensities of various absorption bands of optical absorption spectra. Using these intensity parameters various radiative properties like spontaneous emission probability (A), branching ratio (βR), radiative life time (τ) and stimulated emission cross–section (σp) of various emission lines have been evaluated.

Keywords: ZLSLCBS Glasses, Optical Properties, Judd-Ofelt Theory, Raman spectra.

1. Introduction

Rare earth doped phosphate glasses are being extensively studied due to their technological importance and their applications in the field of glass ceramics, thermal and mechanical sensors, reflecting windows [1-5]. Among different host matrices, silicate glasses are quite prone with the advantages such as low non-linear refractive index, good physical and chemical stability and high transparency from near Ultra Violet to mid-Infrared region [6-11]. Due to their good chemical durability, neodymium-doped soda-lime silicate glasses are attractive materials for the fabrication of low-cost integrated optical amplifiers by using the ion-exchange technique. Glasses contain B2O3 have received increased attention due to their application in the field of glass ceramics, reflecting windows, thermal and mechanical sensors [12-14]. The addition of network modifier (NWF) Li2O is to improve both electrical and mechanical properties of such glasses.  Silicate glasses also exhibit high RE ions solubility [15]. Nd3+ doped materials have proven to be among the most efficient candidates for photonic devices, such as lasers and planer wave guides [16-20].

In the present work, Optical absorption, Excitation, fluorescence and Raman spectra have been recorded at room temperature for all glass samples. From the spectral data various energy interaction parameters like Slater-Condon parameters Fk (k=2, 4, 6), Lande’s parameter ξ4f and Racah parameters Ek (k=1, 2, 3) have been computed. The Judd-Ofelt theory has been applied to compute the intensity parameters Ωλ (λ=2, 4, 6).To understand the laser efficiency of these materials, the value of spectroscopy quality factor (Ω4/ Ω6) has been evaluated.

2. Experimental

The following Nd3+ doped borosilicate glass samples (35-x) SiO2:10ZnO:10Li2O:10CaO:10Na2O:10CdO:15B2O3: xNd2O3.(where x =1, 1.5, 2) have been prepared by melt-quenching method. Analytical reagent grade chemical used in the present study consist of SiO2, ZnO, Li2O, CaO, Na2O, CdO, B2O3 and Nd2O3. They were thoroughly mixed by using an agate pestle mortar. Then melted at 1075˚C by an electrical muffle furnace for 2 hours. After complete melting, the melts were quickly poured in to a preheated stainless steel mould and annealed at temperature of 350˚C for 2 h to remove thermal strains and stresses. Every time fine powder of cerium oxide was used for polishing the samples. The glass samples so prepared were of good optical quality and were transparent. The chemical compositions of the glasses with the name of samples are summarized in Table 1.

Table 1. Chemical composition of the glasses.

Sample                                          Glass composition (mol %)

ZLSLCBS (UD)     35 SiO2:10ZnO:10Li2O:10CaO:10Na2O:10CdO:15B2O3:

ZLSLCBS (ND1)   34SiO2:10ZnO:10Li2O:10CaO:10Na2O:10CdO:15B2O3:1Nd2O3

ZLSLCBS (ND1.5) 33.5SiO2:10ZnO:10Li2O:10CaO:10Na2O:10CdO:15B2O3:1.5Nd2O3

ZLSLCBS (ND2)   33 SiO2:10ZnO:10Li2O:10CaO:10Na2O:10CdO:15B2O3:2Nd2O3

.

ZLSLCBS (UD)-Represents undoped Zinc Lithium Sodalime Cadmium Borosilicate glass specimen.

ZLSLCBS (ND)-Represents Nd3+ doped Zinc Lithium Sodalime Cadmium Borosilicate glass specimens.

III. Theory

3.1Oscillator Strength

The intensity of spectral lines are expressed in terms of oscillator strengths using the relation [21].

fexpt. = 4.318 ×10-9∫ε (ν) dν                                          (1)

where, ε (ν) is molar absorption coefficient at a given energy ν (cm-1), to be evaluated from Beer–Lambert law.

Under Gaussian Approximation, using Beer–Lambert law, the observed oscillator strengths of the absorption bands have been experimentally calculated [22], using the modified relation:

Pm=4.6 ×10-9×log ×Δυ1/2                                     (2)

where c is the molar concentration of the absorbing ion per unit volume, I is the optical path length, logI0/I is optical density and Δυ1/2is half band width.

3.2 Judd-Ofelt Intensity Parameters

According to Judd[23] and Ofelt[24] theory, independently derived expression for the oscillator strength of the induced forced electric dipole transitions between an initial Jmanifold │4fN (S, L) J> level and the terminal J' manifold │4fN (S', L') J'> is given by:

(3)

Where, the line strength S (S', L') is given by the equation

S (J, J') =e2 ∑Ωλ<4f N(S, L) J║U (λ) ║4fN(S', L')J'>2                    (4)

λ =2, 4, 6

In the above equation m is the mass of an electron, c is the velocity of light, ν is the wave number of the transition, h is Planck’s constant, n is the refractive index, J and J' are the total angular momentum of the initial and final level respectively, Ωλ (λ = 2, 4, 6) are known as Judd-Ofelt intensity parameters.

3.3 Radiative Properties

The Ωλ parameters obtained using the absorption spectral results have been used to predict radiative properties such as spontaneous emission probability (A) and radiative life time (τR), and laser parameters like fluorescence branching ratio (βR) and stimulated emission cross section (σp).

The spontaneous emission probability from initial manifold │4fN(S', L') J'> to a final manifold │4fN (S,L) J >| is given by:

A[(S', L') J'; (S,L)J]=64 π2ν33h2J'+1nn2+229×S (J', J)                    (5)

where, S (J', J) = e2 [Ω2║U (2) ║2 + Ω4║U (4) ║2 + Ω6║U (6) ║2]

The fluorescence branching ratio for the transitions originating from a specific initial manifold │4fN (S', L') J'> to a final many fold│4fN (S,L)J > is given by

β[(S', L') J'; ( S , L ) J] =  AS'  LAS' L'J'S  L                                       (6)

S L J

where, the sum is over all terminal manifolds.

The radiative life time is given by

rad A[(S', L') J'; (S,L ) ]  = ATotal-1                         (7)

S L J

where, the sum is over all possible terminal manifolds. The stimulated emission cross -section for a transition from an initial manifold │4fN (S', L') J'> to a final manifold│4fN (S,L)J>| is expressed as

σpλp=λp48πcn2Δλeff×AS',L'J';S, LJ                         (8)

where,λp the peak fluorescence wavelength of the emission band and Δλeff is the effective fluorescence line width.

3.4 Nephelauxetic Ratio (β) and Bonding Parameter (b1/2)

The nature of the R-O bond is known by the Nephelauxetic Ratio (β') and Bonding

Parameters (b1/2), which are computed by using following formulae [25, 26]. The Nephelauxetic Ratio is given by

β'=νgνa                                                                                       (9)

where, νa and νg refer to the energies of the corresponding transition in the glass and free ion, respectively. The values of bonding parameter b1/2 are given by

b1/2=1-β'21/2                                                                          (10)

IV.Result   and Discussion

4.1. XRD Measurement

Figure 1 presents the XRD pattern of the samples shows no sharp Bragg’s peak, but only a broad diffuse hump around low angle region. This is the clear indication of amorphous nature within the resolution limit of XRD instrument.

Fig.1: X-ray diffraction pattern of  SiO2:ZnO:Li2O:CaO:Na2O:CdO:B2O3:  :Nd2O3 glasses.

4.2 Raman spectra

The Raman spectrum of Zinc Lithium Sodalime Cadmium Borosilicate (ZLSLCBS) glass specimens is recorded and is shown in Fig. 2. The spectrum peaks located at 602, 795 and 1204 cm-1. The band at 602 and 795cm-1 assigned to Si–O–Si symmetric stretching and bending vibration, respectively. The band at 1204 cm-1 assigned to Si–O–Si asymmetric stretching.

Fig.2 Raman spectrum of ZLSLCBS ND (01) glass.

4.3. Absorption spectra

The absorption spectra of ZLSLCBS (ND 01) glass, consists of absorption bands corresponding to the absorptions from the ground state 4I9/2 of Nd3+ ions. Nine absorption bands have been observed from the ground state 4I9/2 to excited states 4F3/2, 4F5/2, 4F7/2, 4F9/2, 2H11/2, 4G5/2, 4G7/2, 4G9/2, and 2G9/2 for Nd3+ doped ZLSLCBS (ND 01) glass.

Fig.3: Vis-NIR absorption spectra of ZLSLCBS (ND 01) glass.

The experimental and calculated oscillator strengths for Nd3+ ions in zinc lithium sodalime cadmium borosilicate glasses are given in Table 2.

Table 2. Measured and calculated oscillator strength (Pm × 10+6) of Nd3+ ions in ZLSLCBS glasses.

| Energy level from 4I9/2 | Glass ZLSLCBS (ND01) |  | Glass ZLSLCBS (ND1.5) |  | Glass ZLSLCBS (ND02) |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Pexp. | Pcal. | Pexp. | Pcal. | Pexp. | Pcal. |
| 4F3/2 | 4.38 | 4.03 | 3.42 | 3.38 | 2.64 | 2.76 |
| 4F5/2 | 8.24 | 8.51 | 7.44 | 7.46 | 6.44 | 6.44 |
| 4F7/2 | 8.94 | 9.03 | 7.83 | 8.14 | 6.73 | 7.26 |
| 4F9/2 | 0.64 | 0.51 | 0.55 | 0.45 | 0.43 | 0.40 |
| 2H11/2 | 0.24 | 0.15 | 0.21 | 0.13 | 0.12 | 0.11 |
| 4G5/2 | 25.43 | 25.62 | 24.33 | 24.58 | 23.28 | 23.70 |
| 4G7/2 | 4.68 | 5.44 | 3.89 | 4.81 | 2.63 | 4.21 |
| 4G9/2 | 2.83 | 2.39 | 2.25 | 2.05 | 1.43 | 1.73 |
| 2G9/2 | 0.94 | 3.12 | 0.82 | 2.64 | 0.62 | 2.19 |
| R.m.s.deviation | 0.8009 |  | 0.6981 |  | 0.7811 |  |

The various energy interaction parameters like Slater-Condon parameters Fk (k=2, 4, 6), Lande’s parameter ξ4f , Racah parameters Ek (k=1, 2, 3), nephelauexetic ratio and bonding parameter for Nd3+ doped ZLSLCBS glass specimens are given in Table 3.

Table3. Computed values of Slater-Condon, Lande′, Racah, nephelauexetic ratio and bonding parameter for Nd3+ doped ZLSLCBS glass specimens.

| Parameter | Free ion | ZLSLCBS ( ND01) | ZLSLCBS (ND1.5) | ZLSLCBS ( ND02) |  |
| --- | --- | --- | --- | --- | --- |
| F2(cm-1) | 331.16 | 327.29 | 327.17 | 327.23 |  |
| F4(cm-1) | 50.71 | 49.91 | 49.94 | 49.93 |  |
| F6(cm-1) | 5.154 | 5.137 | 5.131 | 5.134 |  |
| ξ4f(cm-1) | 884.0 | 889.48 | 889.35 | 889.23 |  |
| E1(cm-1) | 5024.0 | 4969.20 | 4967.90 | 4968.78 |  |
| E2(cm-1) | 23.90 | 23.73 | 23.69 | 23.71 |  |
| E3(cm-1) | 497.0 | 489.48 | 489.51 | 489.50 |  |
| F4/F2 | 0.1531 | 0.1525 | 0.1526 | 0.1526 |  |
| F6/F2 | 0.0155 | 1.569 | 0.01568 | 0.01569 |  |
| E1/E3 | 10.1086 | 10.16 | 10.15 | 10.15 |  |
| E2/E3 | 0.0481 | 0.0485 | 0.00484 | 0.00484 |  |
| β' |  | 0.98832 0.0076398 | 0.98796 0.0077583 | 0.988135 0.0077024 |
| b1/2 |  |  |  |  |

Judd-Ofelt intensity parameters Ωλ (λ = 2, 4 and 6) were calculated by using the fitting approximation of the experimental oscillator strengths to the calculated oscillator strengths with respect to their electric dipole contributions. In the present case the three Ωλ parameters follow the trend Ω2 < Ω6 < Ω4.

The values of Judd-Ofelt intensity parameters are given in Table 4.

Table 4. Judd-Ofelt intensity parameters for Nd3+ doped ZLSLCBS glass specimens.

| Glass Specimen | Ω2(pm2) | Ω4(pm2) | Ω6(pm2) | Ω4/Ω6 |  |
| --- | --- | --- | --- | --- | --- |
| ZLSLCBS ( ND01) | 1.718 | 7.945 | 2.848 | 3.204 |  |
| ZLSLCBS (ND1.5) | 2.401 | 6.617 | 2.607 | 2.538 |  |
| ZLSLCBS (ND02) | 3.092 | 5.339 | 2.367 | 2.256 |  |

4.4 Excitation Spectrum

The Excitation spectra of Nd3+doped ZLSLCBS ND (01) glass specimen has been presented in Figure 4 in terms of Excitation Intensity versus wavelength. The excitation spectrum was recorded in the spectral region 700–1000 nm fluorescence at 1065nm having different excitation band centered at 808 nm and 887 nm are attributed to the (4I9/2→4F5/2) and (4I9/2→4F3/2) transitions, respectively. The highest absorption level is 4F5/2 and is at 808 nm. So this is to be chosen for excitation wavelength.

Fig.4: Excitation spectra of ZLSLCBS ND (01) glass

4.5. Fluorescence Spectrum

The fluorescence spectrum of Nd3+doped in zinc lithium sodalime cadmium borosilicate glass is shown in Figure 5. There are six broad bands (4G7/2→4I9/2) (4G7/2→4I11/2), (4F3/2→4I9/2), (4F3/2→4I11/2), (4F3/2→4I13/2) and (4F3/2→4I15/2) respectively for glass specimens.

Fig.5: Fluorescence spectra of ZLSLCBS ND (01) glass.

The wavelengths of these bands along with their assignments are given in Table 5.

Table 5. Emission peak wave lengths (λp), radiative transition probability (Arad), branching ratio (βR), stimulated emission crosssection (σp), and radiative life time (τ) for various transitions in Nd3+ doped ZLSLCBS glasses.

ZLSLCBS (ND01)	                  ZLSLCBS (ND01)                      ZLSLCBS (ND01)

| Transition | λp(nm) | Arad(s-1) | βR | σp (10-20cm2) | τR( μs) | Arad(s-1) | βR | σp (10-20cm2) | τR( μs) | Arad(s-1) | βR | σp (10-20cm2) | τR( μs) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 4G7/2→4I9/2 | 532 | 3877.10 | 0.4422 | 0.494 |  | 3384.80 | 0.4207 | 0.458 |  | 2956.54 | 0.3965 | 0.414 |  |
| 4G7/2→4I11/2 | 595 | 3263.30 | 0.3799 | 1.144 |  | 3309.47 | 0.4114 | 1.231 |  | 3370.14 | 0.4519 | 1.327 |  |
| 4F3/2→4I9/2 | 905 | 983.69 | 0.1133 | 0.866 | 115.22 | 827.30 | 0.1028 | 0.746 | 124.30 | 676.07 | 0.0907 | 0.631 | 134.10 |
| 4F3/2→4I11/2 | 1075 | 517.28 | 0.0596 | 2.174 |  | 452.94 | 0.0563 | 2.035 |  | 389.94 | 0.0523 | 1.884 |  |
| 4F3/2→4I13/2 | 1320 | 75.39 | 0.00869 | 0.378 |  | 69.13 | 0.0085 | 0.366 |  | 62.89 | 0.0084 | 0.345 |  |
| 4F3/2→4I15/2 | 1800 | 1.80 | 0.0002 | 0.0224 |  | 1.65 | 0.0002 | 0.0209 |  | 1.50 | 0.0002 | 0.0194 |  |

V. Conclusion

In the present study, the glass samples of composition (35−x)SiO2:10ZnO: 10Li2O:10CaO:10Na2O:10CdO:15B2O3:xNd2O3 (where x =1, 1.5, 2 mol %) have been prepared by melt-quenching method.  The value of stimulated emission cross-section (σp) is found to be maximum for the transition (4F3/2→4I11/2) for glass ZLSLCBS (ND 01), suggesting that glass ZLSLCBS  (ND 01) is better compared to the other two glass systems ZLSLCBS (ND1.5) and ZLSLCBS (ND02). The large stimulated emission cross section in silicate glasses suggests the possibility of utilizing these systems as laser materials.

References

[1]. Murthy Goud, K. K., Ramesh C.H.  and Rao, B. A.(2017). Up conversion and Spectroscopic Properties of Rare Earth Codoped Lead Borate Glass Matrix.  Material Science Research India, 14, 140-145.

[2].Mohan, S. and Thind, K. S. (2017). Optical and spectroscopic properties of neodymium doped cadmium-sodium borate glasses Opt, Laser Technol. 95, 36–41

[3]. Lin, H., Pun, E.Y.B. and Wang, X.J. et al.(2005). Intense visible fluorescence and energy transfer in Dy3+, Tb3+, Sm3+ and Eu3+ doped rare-earth borate glasses. J. Alloy. Compd., 390,197-201.

[4]. Ramteke, D.D., Annapurna, K., Deshpande, V.K. and Gedam, R.S. (2014).   Effect of Nd3+ on spectroscopic properties of lithium borate glasses. J. Rare Earths 32(12), 1148-1153

[5]. Karthikeyan, B. and Mohan, S. (2003). Structural, optical and glass transition

studies on Nd3+-doped lead bismuth borate glasses, Physica B, 334, 298–302.

[6].Verma, B.R. , Baghel, R.N.(2017). Structural and optical properties of Eu3+

doped silicate phosphors, Indian Journal of Pure Applied Physics, 13, 477-483

[7]. Yasukevich, A. S., Rachkovskaya, G.E., Zakharen, G.B., Trusova,E.E., Kornienko,A. A., Dunina,E.B., Kisel,V. E.and Kuleshov, N. V. (2020).spectral luminescence properties of oxyfluoride lead silicate germante glass doped with Tm3+ ions, Journal of luminescence, 117667.

[8]. Monisha, M., Nancy,A. , Souza,  D., Nimitha ,V. L., Prabhu, S and Sayyed, M.I.(2020). Dy3+ doped SiO2- B2O3-Al2O3-NaF-ZnF2 glasses: An exploration of optical and gamma radiation shielding features, Current Applied Physics 20(11), 1207-1210.

[9]. Chimalawong, P., Kaewkhao, J., Kedkaew, C. and Limsuwan, P. (2010). Optical and ElectronicPolarizability Investigation of Nd3+-Doped Soda-Lime Silicate Glasses. Journal of Physics and Chemistry of Solids, 71, 970.

[10]. Rao,T.G.V.M., Kumar, A. R., Neeraja, K., Veeraiah, N.and Reddy, M.R.(2013).Optical and structural investigation of Eu3+ ions in Nd3+ co-doped magnesium lead borosilicate glasses, J. Alloy. Compd. 557,209–217.

[11]. Berneschi ,S. , Bettinelli ,M., Brenci , M. , Dall’Igna ,R., Nunzi Conti ,G., Pelli ,S., Profilo ,B. , Sebastiani ,S., Speghini , A. and  Righini, G.C.(2006).Optical and spectroscopic properties of soda-lime alumino silicate glasses doped with Er3+ and/or Yb3+, Optical Materials 28,1271–1275

[12]. Li,H. Z., Xin,Y. S., Hua Mao, Ri, H. Chen, Hao, Jun Zhang ,Zhi. and Tai  Zhao, Jing (2014). Luminescence properties of Ce3+-doped lithium borophosphate glasses and their correlations with the optical basicity, Journal of Non-Crystalline Solids 403, 1–4.

[13].Sharma, Y.K., Tandon,S.P. and Surana, S.S.L.(2000).Laser action in praseodymium doped zinc chloride borophosphate glasses. Materials Science and Engineering B77, 167-171.

[14]. Gedam, R. S.and Ramteke, D. D. (2013). Influence of CeO2 addition on the electrical and optical properties of lithium borate glasses, J. Phys. Chem. Solids 74, 1399-1402.

[15]. Weber, M.J. (1990). Science and technology of laser glass. J. Non-Cryst.

Solids, 123, 208–222.

[16]. Dousti, M.R. , Poirier, G.Y.and de Camargo, A.S.S.,(2020).Tungsten Sodium Phosphate glasses doped with trivalent rare earth ions (Eu3+, Tb3+, Nd3+, Er3+ ) for visible and near infrared applications, Journal of Non- Crystalline Solids 530, 119838.

[17]. Reddy, M. S., Uchil, J., Reddy, C. N.(2014).Thermal and Optical properties of Sodium-Phospho- Zinc-Neodymium oxide glass system,  Journal of Advanced Scientific Research, 5(2), 32-39.

[18]. Manasa, P, Srihari, T, Basavapoornima, C., Joshi, A .S. and Jayasankar, C. K .(2019). Spectroscopic investigations of Nd3+ ions in niobium phosphate glasses for laser applicationsJ. Lumin. 211, 233–42.

[19]. Vighnesh, K.R., Ramya, B., Nimitha, S., Wagh,A., Sayyed,  M.I., Sakar,  E., Yakout, H.A. and Dahshan, A. (2020).Structural, optical, thermal, mechanical, morphological and radiation shielding parameters of  Pr3+ doped  ZAIFB glass systems, optical materials 99,109512.

[20]. Campbell, J.H., Suratwala, T.I. (2000).  Nd3+-doped phosphate glasses for high-energy/high-peak-power lasers.J. Non-Cryst. Solids, 263, 318–341.

[21]. Gorller-Walrand, C. and Binnemans, K. (1988) Spectral Intensities of f-f Transition. In: Gshneidner Jr., K.A. and Eyring,L., Eds., Handbook on the Physics and Chemistry of Rare Earths, Vol. 25, Chap. 167, North-Holland, Amsterdam, 101.

[22].Sharma, Y.K., Surana, S.S.L. and Singh, R.K. (2009). Spectroscopic Investigations and Luminescence Spectra of Sm3+ Doped Soda Lime Silicate Glasses. Journal of Rare Earths, 27, 773.

[23].Judd, B.R. (1962). Optical Absorption Intensities of Rare Earth Ions.Physical Review, 127, 750.

[24].Ofelt, G.S. (1962). Intensities of Crystal Spectra of Rare Earth Ions. The Journal of Chemical Physics, 37, 511.

[25].Sinha, S.P. (1983).Systematics and properties of lanthanides, Reidel, Dordrecht.

[26]. Krupke,W.F.(1974).Induced- emission cross-section in neodymium laser glasses. IEEE J. Quantum electron QE-10,450-457.